## Slide 1: Session-Conference ‘Physics of Fundamental Interactions” Department of Physics, Russian Academy of Sciences. 17-21 February 2025, Presidium RAS, Moscow, Russia Simulation of Spectra’s Evolution During Propagation of the Neutron Fluxes in Solid Bodies Sobolevsky N.M., Latysheva L.N., Djilkibaev R.M., Khliustin D.V. Institute for Nuclear Research Russian Academy of Sciences, Moscow, Russia denhlustin@gmail.com
Сессия-конференция Секции ядерной физики Отделения физических наук Российской Академии наук
«Физика фундаментальных взаимодействий», 17-21 февраля 2025 года, Президиум РАН, Москва, Россия

## Slide 2: Abstract
The results of numerical modeling for leakage neutron spectra, for diffusion time and for absorption neutron spectra during propagation of neutron flux in spheres, which consists of nominal density solid bodies of nucleus C12, Ninat and Ta181, are presented. The spherically symmetric task of neutron flux diffusion from a 14.1 MeV central neutron source to the outer surface of spheres, is reviewed. The simulation was carried out using the Monte Carlo code ‘Shield’ [1,2] with 28 energy grouped ABBN-78 neutron constants [3]. The task was carried out within the framework to determine, how material selection choice, for target station of linear accelerator’s proton beam, influences on integral outgoing neutron flux, it’s energy spectrum, and diffusion time. Possibility to recreate capture spectrum of the target station, from experimentally measured by TOF-method leakage neutron spectrum, is being discussed. Obtained calculated data are also necessary to compare with similar data, calculated using 299-group ABBN-93 neutron group constants [4], for calibration purposes. Presented data also can be compared both with experimental leakage neutron TOF spectra measured at the spallation neutron source RADEX, and with calculation results of codes which use introduction of cross sections as continuous curves instead of energy groups.

## Slide 3: Integral experiments are united integral check of all main types of nuclear constants, of cross sections libraries [5] for interactions of neutrons with nuclei. This idea was expressed already in early works [6]. Aim of this work is to describe pure effect of spectrum’s evolution during propagation of the neutron flux inside solid body of chosen material with defined density and known group cross sections [3]. Obtained data allow to compare, how choice of target station’s material influences on outgoing spectrum in neutron guide. As examples of solid body media, in present work we chose as materials spheres of different radiuses: 1.Tantalum isotope Ta181, nominal density solid body metal sphere; 2. Nickel natural isotope composition Ninat metal sphere; 3. Graphite spheres with natural isotope mixture C12 (98.9%) and C13.
Introduction

## Slide 4: Neutron flux inside metal sphere: description of the implemented calculation model
There is a sphere of metal, which has nominal density p, radius 1<R<100 cm and consists of defined isotope or their mixture with known cross sections and matrix of inelastic scattering group transitions [3]. At time t=0 in the center of the sphere are emitted N neutrons which have energy E0, MeV. Must be calculated: * Average time of neutron’s diffusion to external surface of the sphere (when r = R for each neutron); * Energy spectrum of leaking neutron flux, which is flying from sphere’s external surface and can be measured by TOF method; * Energy spectrum of absorbed neutrons.
Start number of neutrons is taken N=1,000,000 for each variant spectrum. Start energy of neutrons is taken E0=14.1 MeV.
Authors also calculated spectrums with start energies 3.0 MeV and 0.6 MeV typical for spallation neutrons and for photonuclear (gamma,n) neutron sources correspondingly. These spectrums with start energies in 3rd and 6th ABBN-78 energy groups allow to appreciate, how results depends on start energy of neutron.

## Slide 5: Neutron cross sections of Ta181 : total cross section (blue line), capture (green), inelastic scattering (red line). Data from the Brookhaven National Laboratory [5].

## Slide 6: ABBN-78 constants for Ta181

## Slide 7: Sphere Ta181 R= 1 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 875382 | 252
0 | 14.0-10.5 MeV | 2439 | 1
1 | 10.5 – 6.5 MeV | 5826 | 0
2 | 6.5 – 4.0 MeV | 9049 | 3
3 | 4.0 – 2.5 MeV | 18340 | 21
4 | 2.5 – 1.4 MeV | 44337 | 149
5 | 1.4 – 0.8 MeV | 58092 | 306
6 | 0.8 – 0.4 MeV | 55514 | 379
7 | 0.4 – 0.2 MeV | 27882 | 281
8 | 0.2 – 0.1 MeV | 9055 | 160
9 | 100 – 46.5 KeV | 2694 | 120
10 | 46.5 – 21.5 KeV | 682 | 34
11 | 21.5 – 10 KeV | 51 | 2
12 | 10 – 4.65 KeV | 12 | 0
13 | 4.65 – 2.15 KeV | 1 | 1
14 | 2.15 – 1 KeV | 1 | 0
15 | 1 – 0.465 KeV | 0 | 0
16 | 465 – 215 eV | 0 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 875382 | 2439 | 5826 | 9049 | 18340 | 44337 | 58092 | 55514 | 27882 | 9055 | 2694 | 682 | 51 | 12 | 1 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 252 | 1 | 0 | 3 | 21 | 149 | 306 | 379 | 281 | 160 | 120 | 34 | 2 | 0 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 8: Sphere Ta181 R= 5 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 501593 | 1002
0 | 14.0-10.5 MeV | 13305 | 12
1 | 10.5 – 6.5 MeV | 14328 | 0
2 | 6.5 – 4.0 MeV | 20623 | 26
3 | 4.0 – 2.5 MeV | 43725 | 427
4 | 2.5 – 1.4 MeV | 116866 | 2719
5 | 1.4 – 0.8 MeV | 190620 | 7162
6 | 0.8 – 0.4 MeV | 239824 | 11055
7 | 0.4 – 0.2 MeV | 158777 | 11328
8 | 0.2 – 0.1 MeV | 64309 | 7850
9 | 100 – 46.5 KeV | 20716 | 5953
10 | 46.5 – 21.5 KeV | 4704 | 2673
11 | 21.5 – 10 KeV | 736 | 617
12 | 10 – 4.65 KeV | 136 | 175
13 | 4.65 – 2.15 KeV | 27 | 42
14 | 2.15 – 1 KeV | 1 | 8
15 | 1 – 0.465 KeV | 0 | 0
16 | 465 – 215 eV | 0 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 501593 | 13305 | 14328 | 20623 | 43725 | 116866 | 190620 | 239824 | 158777 | 64309 | 20716 | 4704 | 736 | 136 | 27 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1002 | 12 | 0 | 26 | 427 | 2719 | 7162 | 11055 | 11328 | 7850 | 5953 | 2673 | 617 | 175 | 42 | 8 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 9: Sphere Ta181 R= 10 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 236268 | 1512
0 | 14.0-10.5 MeV | 20092 | 24
1 | 10.5 – 6.5 MeV | 11498 | 0
2 | 6.5 – 4.0 MeV | 16229 | 58
3 | 4.0 – 2.5 MeV | 33604 | 1014
4 | 2.5 – 1.4 MeV | 96860 | 7233
5 | 1.4 – 0.8 MeV | 188556 | 22463
6 | 0.8 – 0.4 MeV | 309833 | 43039
7 | 0.4 – 0.2 MeV | 288747 | 60412
8 | 0.2 – 0.1 MeV | 150668 | 53869
9 | 100 – 46.5 KeV | 51440 | 45650
10 | 46.5 – 21.5 KeV | 10274 | 18987
11 | 21.5 – 10 KeV | 1692 | 4826
12 | 10 – 4.65 KeV | 236 | 1111
13 | 4.65 – 2.15 KeV | 43 | 246
14 | 2.15 – 1 KeV | 2 | 20
15 | 1 – 0.465 KeV | 0 | 3
16 | 465 – 215 eV | 0 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 236268 | 20092 | 11498 | 16229 | 33604 | 96860 | 188556 | 309833 | 288747 | 150668 | 51440 | 10274 | 1692 | 236 | 43 | 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1512 | 24 | 0 | 58 | 1014 | 7233 | 22463 | 43039 | 60412 | 53869 | 45650 | 18987 | 4826 | 1111 | 246 | 20 | 3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 10: Sphere Ta181 R= 15 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 104660 | 1815
0 | 14.0-10.5 MeV | 19133 | 45
1 | 10.5 – 6.5 MeV | 6813 | 0
2 | 6.5 – 4.0 MeV | 9491 | 90
3 | 4.0 – 2.5 MeV | 19621 | 1373
4 | 2.5 – 1.4 MeV | 57792 | 10591
5 | 1.4 – 0.8 MeV | 125625 | 34876
6 | 0.8 – 0.4 MeV | 249354 | 78468
7 | 0.4 – 0.2 MeV | 302240 | 136324
8 | 0.2 – 0.1 MeV | 194837 | 147959
9 | 100 – 46.5 KeV | 71464 | 136555
10 | 46.5 – 21.5 KeV | 13872 | 55129
11 | 21.5 – 10 KeV | 2005 | 13151
12 | 10 – 4.65 KeV | 234 | 2812
13 | 4.65 – 2.15 KeV | 36 | 732
14 | 2.15 – 1 KeV | 0 | 52
15 | 1 – 0.465 KeV | 1 | 7
16 | 465 – 215 eV | 1 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 104660 | 19133 | 6813 | 9491 | 19621 | 57792 | 125625 | 249354 | 302240 | 194837 | 71464 | 13872 | 2005 | 234 | 36 | 0 | 1 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1815 | 45 | 0 | 90 | 1373 | 10591 | 34876 | 78468 | 136324 | 147959 | 136555 | 55129 | 13151 | 2812 | 732 | 52 | 7 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 11: Sphere Ta181 R= 20 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 44385 | 1929
0 | 14.0-10.5 MeV | 14012 | 73
1 | 10.5 – 6.5 MeV | 3697 | 0
2 | 6.5 – 4.0 MeV | 5039 | 97
3 | 4.0 – 2.5 MeV | 9827 | 1533
4 | 2.5 – 1.4 MeV | 29753 | 12387
5 | 1.4 – 0.8 MeV | 70246 | 43044
6 | 0.8 – 0.4 MeV | 161071 | 104996
7 | 0.4 – 0.2 MeV | 237916 | 206737
8 | 0.2 – 0.1 MeV | 182062 | 256729
9 | 100 – 46.5 KeV | 71741 | 252891
10 | 46.5 – 21.5 KeV | 13658 | 101853
11 | 21.5 – 10 KeV | 1836 | 22921
12 | 10 – 4.65 KeV | 253 | 4609
13 | 4.65 – 2.15 KeV | 21 | 1055
14 | 2.15 – 1 KeV | 0 | 75
15 | 1 – 0.465 KeV | 0 | 12
16 | 465 – 215 eV | 0 | 1
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 44385 | 14012 | 3697 | 5039 | 9827 | 29753 | 70246 | 161071 | 237916 | 182062 | 71741 | 13658 | 1836 | 253 | 21 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1929 | 73 | 0 | 97 | 1533 | 12387 | 43044 | 104996 | 206737 | 256729 | 252891 | 101853 | 22921 | 4609 | 1055 | 75 | 12 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 12: Sphere Ta181 R= 25 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 17935 | 1926
0 | 14.0-10.5 MeV | 8891 | 100
1 | 10.5 – 6.5 MeV | 1832 | 0
2 | 6.5 – 4.0 MeV | 2460 | 106
3 | 4.0 – 2.5 MeV | 4638 | 1614
4 | 2.5 – 1.4 MeV | 14188 | 13341
5 | 1.4 – 0.8 MeV | 35730 | 47903
6 | 0.8 – 0.4 MeV | 92012 | 121866
7 | 0.4 – 0.2 MeV | 157374 | 259709
8 | 0.2 – 0.1 MeV | 139331 | 349476
9 | 100 – 46.5 KeV | 58675 | 358831
10 | 46.5 – 21.5 KeV | 11367 | 144915
11 | 21.5 – 10 KeV | 1437 | 31604
12 | 10 – 4.65 KeV | 185 | 6180
13 | 4.65 – 2.15 KeV | 21 | 1459
14 | 2.15 – 1 KeV | 1 | 102
15 | 1 – 0.465 KeV | 0 | 13
16 | 465 – 215 eV | 0 | 2
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 17935 | 8891 | 1832 | 2460 | 4638 | 14188 | 35730 | 92012 | 157374 | 139331 | 58675 | 11367 | 1437 | 185 | 21 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1926 | 100 | 0 | 106 | 1614 | 13341 | 47903 | 121866 | 259709 | 349476 | 358831 | 144915 | 31604 | 6180 | 1459 | 102 | 13 | 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 13: Sphere Ta181 R= 30 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 6832 | 2064
0 | 14.0-10.5 MeV | 5026 | 114
1 | 10.5 – 6.5 MeV | 910 | 0
2 | 6.5 – 4.0 MeV | 1154 | 98
3 | 4.0 – 2.5 MeV | 2216 | 1650
4 | 2.5 – 1.4 MeV | 6552 | 13629
5 | 1.4 – 0.8 MeV | 17147 | 50169
6 | 0.8 – 0.4 MeV | 47837 | 130685
7 | 0.4 – 0.2 MeV | 94598 | 292229
8 | 0.2 – 0.1 MeV | 92798 | 415298
9 | 100 – 46.5 KeV | 41343 | 440077
10 | 46.5 – 21.5 KeV | 8285 | 178383
11 | 21.5 – 10 KeV | 1033 | 38475
12 | 10 – 4.65 KeV | 108 | 7468
13 | 4.65 – 2.15 KeV | 20 | 1664
14 | 2.15 – 1 KeV | 0 | 129
15 | 1 – 0.465 KeV | 0 | 16
16 | 465 – 215 eV | 0 | 2
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 6832 | 5026 | 910 | 1154 | 2216 | 6552 | 17147 | 47837 | 94598 | 92798 | 41343 | 8285 | 1033 | 108 | 20 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 2064 | 114 | 0 | 98 | 1650 | 13629 | 50169 | 130685 | 292229 | 415298 | 440077 | 178383 | 38475 | 7468 | 1664 | 129 | 16 | 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 14: Sphere Ta181 R= 40 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 959 | 2019
0 | 14.0-10.5 MeV | 1344 | 100
1 | 10.5 – 6.5 MeV | 166 | 0
2 | 6.5 – 4.0 MeV | 248 | 110
3 | 4.0 – 2.5 MeV | 380 | 1663
4 | 2.5 – 1.4 MeV | 1240 | 13908
5 | 1.4 – 0.8 MeV | 3542 | 51891
6 | 0.8 – 0.4 MeV | 11221 | 137234
7 | 0.4 – 0.2 MeV | 26812 | 320797
8 | 0.2 – 0.1 MeV | 32362 | 481645
9 | 100 – 46.5 KeV | 15912 | 527966
10 | 46.5 – 21.5 KeV | 3242 | 215431
11 | 21.5 – 10 KeV | 409 | 45958
12 | 10 – 4.65 KeV | 51 | 8458
13 | 4.65 – 2.15 KeV | 5 | 1929
14 | 2.15 – 1 KeV | 0 | 138
15 | 1 – 0.465 KeV | 0 | 21
16 | 465 – 215 eV | 0 | 2
17 | 215 – 100 eV | 0 | 1
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 959 | 1344 | 166 | 248 | 380 | 1240 | 3542 | 11221 | 26812 | 32362 | 15912 | 3242 | 409 | 51 | 5 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 2019 | 100 | 0 | 110 | 1663 | 13908 | 51891 | 137234 | 320797 | 481645 | 527966 | 215431 | 45958 | 8458 | 1929 | 138 | 21 | 2 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 15: Sphere Ta181 R= 50 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 129 | 2004
0 | 14.0-10.5 MeV | 270 | 126
1 | 10.5 – 6.5 MeV | 33 | 0
2 | 6.5 – 4.0 MeV | 58 | 111
3 | 4.0 – 2.5 MeV | 66 | 1697
4 | 2.5 – 1.4 MeV | 244 | 14105
5 | 1.4 – 0.8 MeV | 675 | 52394
6 | 0.8 – 0.4 MeV | 2232 | 138910
7 | 0.4 – 0.2 MeV | 6433 | 327987
8 | 0.2 – 0.1 MeV | 8936 | 501362
9 | 100 – 46.5 KeV | 4844 | 557217
10 | 46.5 – 21.5 KeV | 985 | 228181
11 | 21.5 – 10 KeV | 110 | 48506
12 | 10 – 4.65 KeV | 13 | 8858
13 | 4.65 – 2.15 KeV | 3 | 1992
14 | 2.15 – 1 KeV | 0 | 147
15 | 1 – 0.465 KeV | 0 | 19
16 | 465 – 215 eV | 0 | 3
17 | 215 – 100 eV | 0 | 1
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 129 | 270 | 33 | 58 | 66 | 244 | 675 | 2232 | 6433 | 8936 | 4844 | 985 | 110 | 13 | 3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 2004 | 126 | 0 | 111 | 1697 | 14105 | 52394 | 138910 | 327987 | 501362 | 557217 | 228181 | 48506 | 8858 | 1992 | 147 | 19 | 3 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 16: Sphere Ta181 R= 65 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 6 | 2000
0 | 14.0-10.5 MeV | 17 | 121
1 | 10.5 – 6.5 MeV | 1 | 0
2 | 6.5 – 4.0 MeV | 2 | 107
3 | 4.0 – 2.5 MeV | 6 | 1715
4 | 2.5 – 1.4 MeV | 17 | 14117
5 | 1.4 – 0.8 MeV | 62 | 52432
6 | 0.8 – 0.4 MeV | 172 | 139380
7 | 0.4 – 0.2 MeV | 629 | 329994
8 | 0.2 – 0.1 MeV | 998 | 507204
9 | 100 – 46.5 KeV | 623 | 566537
10 | 46.5 – 21.5 KeV | 126 | 232389
11 | 21.5 – 10 KeV | 13 | 49229
12 | 10 – 4.65 KeV | 1 | 9016
13 | 4.65 – 2.15 KeV | 0 | 2019
14 | 2.15 – 1 KeV | 0 | 147
15 | 1 – 0.465 KeV | 0 | 19
16 | 465 – 215 eV | 0 | 3
17 | 215 – 100 eV | 0 | 1
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 6 | 17 | 1 | 2 | 6 | 17 | 62 | 172 | 629 | 998 | 623 | 126 | 13 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 2000 | 121 | 0 | 107 | 1715 | 14117 | 52432 | 139380 | 329994 | 507204 | 566537 | 232389 | 49229 | 9016 | 2019 | 147 | 19 | 3 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 17: Sphere Ta181 R= 80 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 1 | 1996
0 | 14.0-10.5 MeV | 2 | 122
1 | 10.5 – 6.5 MeV | 0 | 0
2 | 6.5 – 4.0 MeV | 0 | 107
3 | 4.0 – 2.5 MeV | 0 | 1708
4 | 2.5 – 1.4 MeV | 3 | 14106
5 | 1.4 – 0.8 MeV | 0 | 52499
6 | 0.8 – 0.4 MeV | 14 | 139491
7 | 0.4 – 0.2 MeV | 60 | 330182
8 | 0.2 – 0.1 MeV | 98 | 507775
9 | 100 – 46.5 KeV | 60 | 567549
10 | 46.5 – 21.5 KeV | 12 | 232864
11 | 21.5 – 10 KeV | 2 | 49281
12 | 10 – 4.65 KeV | 0 | 9041
13 | 4.65 – 2.15 KeV | 0 | 2023
14 | 2.15 – 1 KeV | 0 | 148
15 | 1 – 0.465 KeV | 0 | 20
16 | 465 – 215 eV | 0 | 3
17 | 215 – 100 eV | 0 | 1
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1 | 2 | 0 | 0 | 0 | 3 | 0 | 14 | 60 | 98 | 60 | 12 | 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1996 | 122 | 0 | 107 | 1708 | 14106 | 52499 | 139491 | 330182 | 507775 | 567549 | 232864 | 49281 | 9041 | 2023 | 148 | 20 | 3 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 18: Metal sphere Ta181 R= 100 cm Capture spectrum (red curve) Majority of initial 14.1 MeV neutrons in infinite Ta181 media are captured at energies 800 KeV<En<21.5 KeV. It’s necessary to especially note, that maximum of both spectra is below 100 KeV i.e. neutron fluxes such energies already can be measured by existing TOF spectrometers.
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 0 | 1994
0 | 14.0-10.5 MeV | 0 | 122
1 | 10.5 – 6.5 MeV | 0 | 0
2 | 6.5 – 4.0 MeV | 0 | 107
3 | 4.0 – 2.5 MeV | 0 | 1708
4 | 2.5 – 1.4 MeV | 0 | 14099
5 | 1.4 – 0.8 MeV | 0 | 52500
6 | 0.8 – 0.4 MeV | 0 | 139495
7 | 0.4 – 0.2 MeV | 1 | 330214
8 | 0.2 – 0.1 MeV | 3 | 507853
9 | 100 – 46.5 KeV | 3 | 567658
10 | 46.5 – 21.5 KeV | 1 | 232902
11 | 21.5 – 10 KeV | 0 | 49298
12 | 10 – 4.65 KeV | 0 | 9047
13 | 4.65 – 2.15 KeV | 0 | 2027
14 | 2.15 – 1 KeV | 0 | 148
15 | 1 – 0.465 KeV | 0 | 20
16 | 465 – 215 eV | 0 | 3
17 | 215 – 100 eV | 0 | 1
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1994 | 122 | 0 | 107 | 1708 | 14099 | 52500 | 139495 | 330214 | 507853 | 567658 | 232902 | 49298 | 9047 | 2027 | 148 | 20 | 3 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 19: Spectrums in metal Tantalum Ta181 spheres
ABBN-78 Group № | Energy Interval | R = 1 cm |  | R = 5 cm |  | R = 10 cm |  | R = 15 cm |  | R = 20 cm |  | R = 25 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 875382 | 252 | 501593 | 1002 | 236268 | 1512 | 104660 | 1815 | 44385 | 1929 | 17935 | 1926
0 | 14.0-10.5 MeV | 2439 | 1 | 13305 | 12 | 20092 | 24 | 19133 | 45 | 14012 | 73 | 8891 | 100
1 | 10.5-6.5 MeV | 5826 | 0 | 14328 | 0 | 11498 | 0 | 6813 | 0 | 3697 | 0 | 1832 | 0
2 | 6.5-4.0 MeV | 9049 | 3 | 20623 | 26 | 16229 | 58 | 9491 | 90 | 5039 | 97 | 2460 | 106
3 | 4.0-2.5 MeV | 18340 | 21 | 43725 | 427 | 33604 | 1014 | 19621 | 1373 | 9827 | 1533 | 4638 | 1614
4 | 2.5-1.4 MeV | 44337 | 149 | 116866 | 2719 | 96860 | 7233 | 57792 | 10591 | 29753 | 12387 | 14188 | 13341
5 | 1.4-0.8 MeV | 58092 | 306 | 190620 | 7162 | 188556 | 22463 | 125625 | 34876 | 70246 | 43044 | 35730 | 47903
6 | 0.8-0.4 MeV | 55514 | 379 | 239824 | 11055 | 309833 | 43039 | 249354 | 78468 | 161071 | 104996 | 92012 | 121866
7 | 0.4-0.2 MeV | 27882 | 281 | 158777 | 11328 | 288747 | 60412 | 302240 | 136324 | 237916 | 206737 | 157374 | 259709
8 | 0.2-0.1 MeV | 9055 | 160 | 64309 | 7850 | 150668 | 53869 | 194837 | 147959 | 182062 | 256729 | 139331 | 349476
9 | 100-46.5 KeV | 2694 | 120 | 20716 | 5953 | 51440 | 45650 | 71464 | 136555 | 71741 | 252891 | 58675 | 358831
10 | 46.5 –21.5 KeV | 682 | 34 | 4704 | 2673 | 10274 | 18987 | 13872 | 55129 | 13658 | 101853 | 11367 | 144915
11 | 21.5– 10 KeV | 51 | 2 | 736 | 617 | 1692 | 4826 | 2005 | 13151 | 1836 | 22921 | 1437 | 31604
12 | 10– 4.65 KeV | 12 | 0 | 136 | 175 | 236 | 1111 | 234 | 2812 | 253 | 4609 | 185 | 6180
13 | 4.65– 2.15 KeV | 1 | 1 | 27 | 42 | 43 | 246 | 36 | 732 | 21 | 1055 | 21 | 1459
14 | 2.15 – 1 KeV | 1 | 0 | 1 | 8 | 2 | 20 | 0 | 52 | 0 | 75 | 1 | 102
15 | 1– 0.465 KeV | 0 | 0 | 0 | 0 | 0 | 3 | 1 | 7 | 0 | 12 | 0 | 13
16 | 465– 215 eV | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 1 | 0 | 2
17 | 215– 100 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
18 | 100– 46.5 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
19 | 46.5– 21.5 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
20 | 21.5– 10 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
21 | 10– 4.65 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
22 | 4.6 – 2.15 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
23 | 2.1 – 1.0 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
24 | 1.0– 0.465 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
25 | 0.46 – 0.215 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
26 | 0.215– 0.001 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Average Neutron Energy |  | 11.40 MeV | 2.70 MeV | 5.90 MeV | 785 KeV | 3.20 MeV | 444 KeV | 2.03 MeV | 327 KeV | 1.44 MeV | 273 KeV | 1.095 MeV | 246 KeV
Diffusion/Absorption time of spectra, nanoseconds |  | 0.337 | 0.776 | 4.68 | 9.05 | 16.73 | 28.21 | 32.99 | 49.03 | 49.94 | 66.03 | 66.57 | 78.26
Number of neutrons |  | 1109357 | 1709 | 1390290 | 51049 | 1416042 | 260467 | 1177179 | 619979 | 845517 | 1010942 | 546077 | 1339147

## Slide 20: Spectrums in metal Tantalum Ta181 spheres
ABBN-78 Group № | Energy Interval | R = 30 cm |  | R = 40 cm |  | R = 50 cm |  | R = 65 cm |  | R = 80 cm |  | R = 100 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 6832 | 2064 | 959 | 2019 | 129 | 2004 | 6 | 2000 | 1 | 1996 | 0 | 1994
0 | 14.0-10.5 MeV | 5026 | 114 | 1344 | 100 | 270 | 126 | 17 | 121 | 2 | 122 | 0 | 122
1 | 10.5-6.5 MeV | 910 | 0 | 166 | 0 | 33 | 0 | 1 | 0 | 0 | 0 | 0 | 0
2 | 6.5-4.0 MeV | 1154 | 98 | 248 | 110 | 58 | 111 | 2 | 107 | 0 | 107 | 0 | 107
3 | 4.0-2.5 MeV | 2216 | 1650 | 380 | 1663 | 66 | 1697 | 6 | 1715 | 0 | 1708 | 0 | 1708
4 | 2.5-1.4 MeV | 6552 | 13629 | 1240 | 13908 | 244 | 14105 | 17 | 14117 | 3 | 14106 | 0 | 14099
5 | 1.4-0.8 MeV | 17147 | 50169 | 3542 | 51891 | 675 | 52394 | 62 | 52432 | 0 | 52499 | 0 | 52500
6 | 0.8-0.4 MeV | 47837 | 130685 | 11221 | 137234 | 2232 | 138910 | 172 | 139380 | 14 | 139491 | 0 | 139495
7 | 0.4-0.2 MeV | 94598 | 292229 | 26812 | 320797 | 6433 | 327987 | 629 | 329994 | 60 | 330182 | 1 | 330214
8 | 0.2-0.1 MeV | 92798 | 415298 | 32362 | 481645 | 8936 | 501362 | 998 | 507204 | 98 | 507775 | 3 | 507853
9 | 100-46.5 KeV | 41343 | 440077 | 15912 | 527966 | 4844 | 557217 | 623 | 566537 | 60 | 567549 | 3 | 567658
10 | 46.5 –21.5 KeV | 8285 | 178383 | 3242 | 215431 | 985 | 228181 | 126 | 232389 | 12 | 232864 | 1 | 232902
11 | 21.5– 10 KeV | 1033 | 38475 | 409 | 45958 | 110 | 48506 | 13 | 49229 | 2 | 49281 | 0 | 49298
12 | 10– 4.65 KeV | 108 | 7468 | 51 | 8458 | 13 | 8858 | 1 | 9016 | 0 | 9041 | 0 | 9047
13 | 4.65– 2.15 KeV | 20 | 1664 | 5 | 1929 | 3 | 1992 | 0 | 2019 | 0 | 2023 | 0 | 2027
14 | 2.15 – 1 KeV | 0 | 129 | 0 | 138 | 0 | 147 | 0 | 147 | 0 | 148 | 0 | 148
15 | 1– 0.465 KeV | 0 | 16 | 0 | 21 | 0 | 19 | 0 | 19 | 0 | 20 | 0 | 20
16 | 465– 215 eV | 0 | 2 | 0 | 2 | 0 | 3 | 0 | 3 | 0 | 3 | 0 | 3
17 | 215– 100 eV | 0 | 0 | 0 | 1 | 0 | 1 | 0 | 1 | 0 | 1 | 0 | 1
18 | 100– 46.5 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
19 | 46.5– 21.5 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
20 | 21.5– 10 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
21 | 10– 4.65 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
22 | 4.6 – 2.15 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
23 | 2.1 – 1.0 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
24 | 1.0– 0.465 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
25 | 0.46 – 0.215 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
26 | 0.215– 0.001 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Average Neutron Energy |  | 870 KeV | 232 KeV | 621 KeV | 218 KeV | 479 KeV | 215 KeV | 332 KeV | 213 KeV | 343 KeV | 213 KeV | 109 KeV | 213 KeV
Diffusion/Absorption time of spectra, nanoseconds |  | 82.18 | 86.93 | 111.59 | 96.57 | 137.07 | 100.26 | 173.84 | 101.67 | 197.15 | 101.91 | 215.88 | 101.88
Number of neutrons |  | 325859 | 1572150 | 97893 | 1809271 | 25031 | 1883620 | 2673 | 1906430 | 252 | 1908916 | 8 | 1909196

## Slide 21
Ni61 (1.25% in Ninat)
Ni62 (3.66% in Ninat)
Ni64 (1.16% in Ninat)
Neutron cross sections of isotopes of Ninat : total cross section (blue line), capture (green), inelastic scattering (red line). Data from the Brookhaven National Laboratory [5].
Ni58 (67.76% in Ninat)
Ni60 (26.16% in Ninat)

## Slide 22: ABBN-78 constants for 28Ninat

## Slide 23: Sphere of Nickel Ninat R= 1 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 855171 | 38129
0 | 14.0-10.5 MeV | 14702 | 502
1 | 10.5 – 6.5 MeV | 12915 | 531
2 | 6.5 – 4.0 MeV | 22591 | 647
3 | 4.0 – 2.5 MeV | 25269 | 334
4 | 2.5 – 1.4 MeV | 21138 | 81
5 | 1.4 – 0.8 MeV | 12632 | 77
6 | 0.8 – 0.4 MeV | 5956 | 0
7 | 0.4 – 0.2 MeV | 2430 | 3
8 | 0.2 – 0.1 MeV | 283 | 0
9 | 100 – 46.5 KeV | 96 | 0
10 | 46.5 – 21.5 KeV | 0 | 0
11 | 21.5 – 10 KeV | 0 | 0
12 | 10 – 4.65 KeV | 0 | 0
13 | 4.65 – 2.15 KeV | 0 | 0
14 | 2.15 – 1 KeV | 0 | 0
15 | 1 – 0.465 KeV | 0 | 0
16 | 465 – 215 eV | 0 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 855171 | 14702 | 12915 | 22591 | 25269 | 21138 | 12632 | 5956 | 2430 | 283 | 96 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 38129 | 502 | 531 | 647 | 334 | 81 | 77 | 0 | 3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 24: Sphere of Nickel Ninat R= 5 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 450166 | 142319
0 | 14.0-10.5 MeV | 42000 | 9147
1 | 10.5 – 6.5 MeV | 27704 | 7996
2 | 6.5 – 4.0 MeV | 50266 | 10105
3 | 4.0 – 2.5 MeV | 69927 | 5872
4 | 2.5 – 1.4 MeV | 84013 | 1806
5 | 1.4 – 0.8 MeV | 73447 | 365
6 | 0.8 – 0.4 MeV | 46477 | 212
7 | 0.4 – 0.2 MeV | 19851 | 154
8 | 0.2 – 0.1 MeV | 6586 | 82
9 | 100 – 46.5 KeV | 1998 | 54
10 | 46.5 – 21.5 KeV | 353 | 12
11 | 21.5 – 10 KeV | 9 | 4
12 | 10 – 4.65 KeV | 39 | 0
13 | 4.65 – 2.15 KeV | 7 | 0
14 | 2.15 – 1 KeV | 1 | 0
15 | 1 – 0.465 KeV | 0 | 0
16 | 465 – 215 eV | 2 | 0
17 | 215 – 100 eV | 1 | 0
18 | 100 – 46.5 eV | 2 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 450166 | 42000 | 27704 | 50266 | 69927 | 84013 | 73447 | 46477 | 19851 | 6586 | 1998 | 353 | 9 | 39 | 7 | 1 | 0 | 2 | 1 | 2 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 142319 | 9147 | 7996 | 10105 | 5872 | 1806 | 365 | 212 | 154 | 82 | 54 | 12 | 4 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 25: Sphere of Nickel Ninat R= 10 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 194766 | 206527
0 | 14.0-10.5 MeV | 41196 | 23213
1 | 10.5 – 6.5 MeV | 20216 | 17815
2 | 6.5 – 4.0 MeV | 35792 | 23643
3 | 4.0 – 2.5 MeV | 60063 | 15499
4 | 2.5 – 1.4 MeV | 101659 | 6164
5 | 1.4 – 0.8 MeV | 129886 | 1747
6 | 0.8 – 0.4 MeV | 110650 | 1397
7 | 0.4 – 0.2 MeV | 45453 | 998
8 | 0.2 – 0.1 MeV | 22918 | 882
9 | 100 – 46.5 KeV | 7540 | 578
10 | 46.5 – 21.5 KeV | 2453 | 370
11 | 21.5 – 10 KeV | 145 | 151
12 | 10 – 4.65 KeV | 758 | 53
13 | 4.65 – 2.15 KeV | 308 | 55
14 | 2.15 – 1 KeV | 327 | 60
15 | 1 – 0.465 KeV | 198 | 31
16 | 465 – 215 eV | 118 | 24
17 | 215 – 100 eV | 86 | 31
18 | 100 – 46.5 eV | 70 | 33
19 | 46.5 – 21.5 eV | 40 | 23
20 | 21.5 – 10 eV | 31 | 36
21 | 10 – 4.65 eV | 16 | 29
22 | 4.65 – 2.15 eV | 2 | 12
23 | 2.15 – 1.0 eV | 3 | 10
24 | 1.0 – 0.465 eV | 1 | 7
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 194766 | 41196 | 20216 | 35792 | 60063 | 101659 | 129886 | 110650 | 45453 | 22918 | 7540 | 2453 | 145 | 758 | 308 | 327 | 198 | 118 | 86 | 70 | 40 | 31 | 16 | 2 | 3 | 1 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 206527 | 23213 | 17815 | 23643 | 15499 | 6164 | 1747 | 1397 | 998 | 882 | 578 | 370 | 151 | 53 | 55 | 60 | 31 | 24 | 31 | 33 | 23 | 36 | 29 | 12 | 10 | 7 | 0 | 0

## Slide 26: Sphere of Nickel Ninat R= 15 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 81574 | 233769
0 | 14.0-10.5 MeV | 28894 | 34452
1 | 10.5 – 6.5 MeV | 10797 | 24270
2 | 6.5 – 4.0 MeV | 19060 | 30944
3 | 4.0 – 2.5 MeV | 36823 | 22946
4 | 2.5 – 1.4 MeV | 82094 | 10911
5 | 1.4 – 0.8 MeV | 141048 | 4079
6 | 0.8 – 0.4 MeV | 160519 | 3982
7 | 0.4 – 0.2 MeV | 66310 | 3075
8 | 0.2 – 0.1 MeV | 40876 | 3356
9 | 100 – 46.5 KeV | 16249 | 2643
10 | 46.5 – 21.5 KeV | 6150 | 2030
11 | 21.5 – 10 KeV | 523 | 939
12 | 10 – 4.65 KeV | 2619 | 414
13 | 4.65 – 2.15 KeV | 1203 | 557
14 | 2.15 – 1 KeV | 1355 | 509
15 | 1 – 0.465 KeV | 1119 | 322
16 | 465 – 215 eV | 956 | 366
17 | 215 – 100 eV | 730 | 424
18 | 100 – 46.5 eV | 597 | 531
19 | 46.5 – 21.5 eV | 437 | 588
20 | 21.5 – 10 eV | 304 | 671
21 | 10 – 4.65 eV | 215 | 616
22 | 4.65 – 2.15 eV | 128 | 507
23 | 2.15 – 1.0 eV | 51 | 382
24 | 1.0 – 0.465 eV | 15 | 205
25 | 0.465 – 0.215 eV | 3 | 90
26 | 0.215 – 0.001 eV | 0 | 9
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 81574 | 28894 | 10797 | 19060 | 36823 | 82094 | 141048 | 160519 | 66310 | 40876 | 16249 | 6150 | 523 | 2619 | 1203 | 1355 | 1119 | 956 | 730 | 597 | 437 | 304 | 215 | 128 | 51 | 15 | 3 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 233769 | 34452 | 24270 | 30944 | 22946 | 10911 | 4079 | 3982 | 3075 | 3356 | 2643 | 2030 | 939 | 414 | 557 | 509 | 322 | 366 | 424 | 531 | 588 | 671 | 616 | 507 | 382 | 205 | 90 | 9

## Slide 27: Sphere of Nickel Ninat R= 20 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 33423 | 244697
0 | 14.0-10.5 MeV | 17527 | 41597
1 | 10.5 – 6.5 MeV | 5292 | 27506
2 | 6.5 – 4.0 MeV | 9147 | 35056
3 | 4.0 – 2.5 MeV | 19677 | 27119
4 | 2.5 – 1.4 MeV | 53721 | 14641
5 | 1.4 – 0.8 MeV | 118846 | 6247
6 | 0.8 – 0.4 MeV | 179442 | 7653
7 | 0.4 – 0.2 MeV | 79291 | 6149
8 | 0.2 – 0.1 MeV | 53821 | 7747
9 | 100 – 46.5 KeV | 24119 | 6884
10 | 46.5 – 21.5 KeV | 10111 | 6038
11 | 21.5 – 10 KeV | 893 | 2931
12 | 10 – 4.65 KeV | 4814 | 1316
13 | 4.65 – 2.15 KeV | 2363 | 1954
14 | 2.15 – 1 KeV | 2840 | 1809
15 | 1 – 0.465 KeV | 2333 | 1178
16 | 465 – 215 eV | 2118 | 1528
17 | 215 – 100 eV | 1789 | 1886
18 | 100 – 46.5 eV | 1507 | 2448
19 | 46.5 – 21.5 eV | 1240 | 2837
20 | 21.5 – 10 eV | 952 | 3132
21 | 10 – 4.65 eV | 637 | 3166
22 | 4.65 – 2.15 eV | 414 | 2833
23 | 2.15 – 1.0 eV | 182 | 2142
24 | 1.0 – 0.465 eV | 59 | 1169
25 | 0.465 – 0.215 eV | 17 | 421
26 | 0.215 – 0.001 eV | 0 | 98
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 33423 | 17527 | 5292 | 9147 | 19677 | 53721 | 118846 | 179442 | 79291 | 53821 | 24119 | 10111 | 893 | 4814 | 2363 | 2840 | 2333 | 2118 | 1789 | 1507 | 1240 | 952 | 637 | 414 | 182 | 59 | 17 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 244697 | 41597 | 27506 | 35056 | 27119 | 14641 | 6247 | 7653 | 6149 | 7747 | 6884 | 6038 | 2931 | 1316 | 1954 | 1809 | 1178 | 1528 | 1886 | 2448 | 2837 | 3132 | 3166 | 2833 | 2142 | 1169 | 421 | 98

## Slide 28: Sphere of Nickel Ninat R= 25 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 13413 | 250264
0 | 14.0-10.5 MeV | 9806 | 45677
1 | 10.5 – 6.5 MeV | 2457 | 28865
2 | 6.5 – 4.0 MeV | 4064 | 37242
3 | 4.0 – 2.5 MeV | 9437 | 29315
4 | 2.5 – 1.4 MeV | 32203 | 16570
5 | 1.4 – 0.8 MeV | 86346 | 7728
6 | 0.8 – 0.4 MeV | 166124 | 11458
7 | 0.4 – 0.2 MeV | 81613 | 10096
8 | 0.2 – 0.1 MeV | 58290 | 13223
9 | 100 – 46.5 KeV | 28469 | 13221
10 | 46.5 – 21.5 KeV | 12768 | 12073
11 | 21.5 – 10 KeV | 1217 | 6086
12 | 10 – 4.65 KeV | 6323 | 2820
13 | 4.65 – 2.15 KeV | 3103 | 4229
14 | 2.15 – 1 KeV | 4033 | 4199
15 | 1 – 0.465 KeV | 3399 | 2697
16 | 465 – 215 eV | 3016 | 3720
17 | 215 – 100 eV | 2555 | 4639
18 | 100 – 46.5 eV | 2333 | 5930
19 | 46.5 – 21.5 eV | 1925 | 7285
20 | 21.5 – 10 eV | 1519 | 8389
21 | 10 – 4.65 eV | 1071 | 8771
22 | 4.65 – 2.15 eV | 634 | 8084
23 | 2.15 – 1.0 eV | 335 | 6033
24 | 1.0 – 0.465 eV | 144 | 3301
25 | 0.465 – 0.215 eV | 43 | 1262
26 | 0.215 – 0.001 eV | 2 | 335
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 13413 | 9806 | 2457 | 4064 | 9437 | 32203 | 86346 | 166124 | 81613 | 58290 | 28469 | 12768 | 1217 | 6323 | 3103 | 4033 | 3399 | 3016 | 2555 | 2333 | 1925 | 1519 | 1071 | 634 | 335 | 144 | 43 | 2
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 250264 | 45677 | 28865 | 37242 | 29315 | 16570 | 7728 | 11458 | 10096 | 13223 | 13221 | 12073 | 6086 | 2820 | 4229 | 4199 | 2697 | 3720 | 4639 | 5930 | 7285 | 8389 | 8771 | 8084 | 6033 | 3301 | 1262 | 335

## Slide 29: Sphere of Nickel Ninat R= 30 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 5306 | 251973
0 | 14.0-10.5 MeV | 5146 | 48052
1 | 10.5 – 6.5 MeV | 1104 | 29602
2 | 6.5 – 4.0 MeV | 1817 | 38148
3 | 4.0 – 2.5 MeV | 4495 | 30139
4 | 2.5 – 1.4 MeV | 17685 | 17913
5 | 1.4 – 0.8 MeV | 56539 | 8912
6 | 0.8 – 0.4 MeV | 134926 | 14768
7 | 0.4 – 0.2 MeV | 75659 | 13869
8 | 0.2 – 0.1 MeV | 56635 | 19321
9 | 100 – 46.5 KeV | 28717 | 20097
10 | 46.5 – 21.5 KeV | 13647 | 19288
11 | 21.5 – 10 KeV | 1213 | 9672
12 | 10 – 4.65 KeV | 7013 | 4653
13 | 4.65 – 2.15 KeV | 3555 | 7049
14 | 2.15 – 1 KeV | 4538 | 6951
15 | 1 – 0.465 KeV | 3772 | 4566
16 | 465 – 215 eV | 3624 | 6414
17 | 215 – 100 eV | 3290 | 8103
18 | 100 – 46.5 eV | 2820 | 10719
19 | 46.5 – 21.5 eV | 2409 | 13509
20 | 21.5 – 10 eV | 1840 | 15621
21 | 10 – 4.65 eV | 1400 | 16368
22 | 4.65 – 2.15 eV | 875 | 15075
23 | 2.15 – 1.0 eV | 433 | 11614
24 | 1.0 – 0.465 eV | 171 | 6721
25 | 0.465 – 0.215 eV | 36 | 2596
26 | 0.215 – 0.001 eV | 5 | 637
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 5306 | 5146 | 1104 | 1817 | 4495 | 17685 | 56539 | 134926 | 75659 | 56635 | 28717 | 13647 | 1213 | 7013 | 3555 | 4538 | 3772 | 3624 | 3290 | 2820 | 2409 | 1840 | 1400 | 875 | 433 | 171 | 36 | 5
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 251973 | 48052 | 29602 | 38148 | 30139 | 17913 | 8912 | 14768 | 13869 | 19321 | 20097 | 19288 | 9672 | 4653 | 7049 | 6951 | 4566 | 6414 | 8103 | 10719 | 13509 | 15621 | 16368 | 15075 | 11614 | 6721 | 2596 | 637

## Slide 30: Sphere of Nickel Ninat R= 40 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 799 | 252566
0 | 14.0-10.5 MeV | 1213 | 49787
1 | 10.5 – 6.5 MeV | 209 | 30040
2 | 6.5 – 4.0 MeV | 324 | 38788
3 | 4.0 – 2.5 MeV | 915 | 31372
4 | 2.5 – 1.4 MeV | 4701 | 18989
5 | 1.4 – 0.8 MeV | 20074 | 10218
6 | 0.8 – 0.4 MeV | 69853 | 19169
7 | 0.4 – 0.2 MeV | 49006 | 20120
8 | 0.2 – 0.1 MeV | 40244 | 29705
9 | 100 – 46.5 KeV | 22190 | 32125
10 | 46.5 – 21.5 KeV | 10850 | 32815
11 | 21.5 – 10 KeV | 1035 | 16903
12 | 10 – 4.65 KeV | 5850 | 8137
13 | 4.65 – 2.15 KeV | 2983 | 12852
14 | 2.15 – 1 KeV | 3810 | 12628
15 | 1 – 0.465 KeV | 3406 | 8510
16 | 465 – 215 eV | 3185 | 11829
17 | 215 – 100 eV | 2973 | 15684
18 | 100 – 46.5 eV | 2662 | 20328
19 | 46.5 – 21.5 eV | 2335 | 25891
20 | 21.5 – 10 eV | 1842 | 30492
21 | 10 – 4.65 eV | 1361 | 32755
22 | 4.65 – 2.15 eV | 837 | 31212
23 | 2.15 – 1.0 eV | 461 | 24105
24 | 1.0 – 0.465 eV | 171 | 13928
25 | 0.465 – 0.215 eV | 44 | 5444
26 | 0.215 – 0.001 eV | 3 | 1409
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 799 | 1213 | 209 | 324 | 915 | 4701 | 20074 | 69853 | 49006 | 40244 | 22190 | 10850 | 1035 | 5850 | 2983 | 3810 | 3406 | 3185 | 2973 | 2662 | 2335 | 1842 | 1361 | 837 | 461 | 171 | 44 | 3
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 252566 | 49787 | 30040 | 38788 | 31372 | 18989 | 10218 | 19169 | 20120 | 29705 | 32125 | 32815 | 16903 | 8137 | 12852 | 12628 | 8510 | 11829 | 15684 | 20328 | 25891 | 30492 | 32755 | 31212 | 24105 | 13928 | 5444 | 1409

## Slide 31: Sphere of Nickel Ninat R= 65 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 6 | 253196
0 | 14.0-10.5 MeV | 29 | 50393
1 | 10.5 – 6.5 MeV | 3 | 30189
2 | 6.5 – 4.0 MeV | 2 | 38985
3 | 4.0 – 2.5 MeV | 14 | 31417
4 | 2.5 – 1.4 MeV | 123 | 19255
5 | 1.4 – 0.8 MeV | 772 | 10702
6 | 0.8 – 0.4 MeV | 5568 | 21914
7 | 0.4 – 0.2 MeV | 6073 | 25355
8 | 0.2 – 0.1 MeV | 6539 | 39331
9 | 100 – 46.5 KeV | 4206 | 45299
10 | 46.5 – 21.5 KeV | 2189 | 47991
11 | 21.5 – 10 KeV | 212 | 25062
12 | 10 – 4.65 KeV | 1233 | 12191
13 | 4.65 – 2.15 KeV | 668 | 19555
14 | 2.15 – 1 KeV | 867 | 19547
15 | 1 – 0.465 KeV | 755 | 13159
16 | 465 – 215 eV | 785 | 18567
17 | 215 – 100 eV | 673 | 24973
18 | 100 – 46.5 eV | 673 | 32842
19 | 46.5 – 21.5 eV | 571 | 42489
20 | 21.5 – 10 eV | 498 | 50069
21 | 10 – 4.65 eV | 349 | 55013
22 | 4.65 – 2.15 eV | 234 | 52935
23 | 2.15 – 1.0 eV | 133 | 41259
24 | 1.0 – 0.465 eV | 54 | 24156
25 | 0.465 – 0.215 eV | 9 | 9651
26 | 0.215 – 0.001 eV | 2 | 2604
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 6 | 29 | 3 | 2 | 14 | 123 | 772 | 5568 | 6073 | 6539 | 4206 | 2189 | 212 | 1233 | 668 | 867 | 755 | 785 | 673 | 673 | 571 | 498 | 349 | 234 | 133 | 54 | 9 | 2
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 253196 | 50393 | 30189 | 38985 | 31417 | 19255 | 10702 | 21914 | 25355 | 39331 | 45299 | 47991 | 25062 | 12191 | 19555 | 19547 | 13159 | 18567 | 24973 | 32842 | 42489 | 50069 | 55013 | 52935 | 41259 | 24156 | 9651 | 2604

## Slide 32: Sphere of Nickel Ninat R= 80 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 1 | 253034
0 | 14.0-10.5 MeV | 4 | 50438
1 | 10.5 – 6.5 MeV | 0 | 30051
2 | 6.5 – 4.0 MeV | 0 | 39086
3 | 4.0 – 2.5 MeV | 0 | 31349
4 | 2.5 – 1.4 MeV | 10 | 19194
5 | 1.4 – 0.8 MeV | 103 | 10713
6 | 0.8 – 0.4 MeV | 887 | 22004
7 | 0.4 – 0.2 MeV | 1169 | 25733
8 | 0.2 – 0.1 MeV | 1410 | 40306
9 | 100 – 46.5 KeV | 977 | 46729
10 | 46.5 – 21.5 KeV | 552 | 49568
11 | 21.5 – 10 KeV | 55 | 25866
12 | 10 – 4.65 KeV | 327 | 12664
13 | 4.65 – 2.15 KeV | 170 | 20371
14 | 2.15 – 1 KeV | 236 | 20305
15 | 1 – 0.465 KeV | 196 | 13620
16 | 465 – 215 eV | 222 | 19339
17 | 215 – 100 eV | 196 | 25919
18 | 100 – 46.5 eV | 155 | 34524
19 | 46.5 – 21.5 eV | 173 | 44763
20 | 21.5 – 10 eV | 132 | 52770
21 | 10 – 4.65 eV | 93 | 58062
22 | 4.65 – 2.15 eV | 67 | 55854
23 | 2.15 – 1.0 eV | 32 | 43392
24 | 1.0 – 0.465 eV | 11 | 25499
25 | 0.465 – 0.215 eV | 2 | 10241
26 | 0.215 – 0.001 eV | 0 | 2757
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1 | 4 | 0 | 0 | 0 | 10 | 103 | 887 | 1169 | 1410 | 977 | 552 | 55 | 327 | 170 | 236 | 196 | 222 | 196 | 155 | 173 | 132 | 93 | 67 | 32 | 11 | 2 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 253034 | 50438 | 30051 | 39086 | 31349 | 19194 | 10713 | 22004 | 25733 | 40306 | 46729 | 49568 | 25866 | 12664 | 20371 | 20305 | 13620 | 19339 | 25919 | 34524 | 44763 | 52770 | 58062 | 55854 | 43392 | 25499 | 10241 | 2757

## Slide 33: Sphere of Nickel Ninat R= 100 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 0 | 252935
0 | 14.0-10.5 MeV | 0 | 50467
1 | 10.5 – 6.5 MeV | 0 | 30104
2 | 6.5 – 4.0 MeV | 0 | 39034
3 | 4.0 – 2.5 MeV | 0 | 31327
4 | 2.5 – 1.4 MeV | 0 | 19175
5 | 1.4 – 0.8 MeV | 6 | 10748
6 | 0.8 – 0.4 MeV | 39 | 22076
7 | 0.4 – 0.2 MeV | 92 | 25809
8 | 0.2 – 0.1 MeV | 134 | 40473
9 | 100 – 46.5 KeV | 97 | 47003
10 | 46.5 – 21.5 KeV | 53 | 49961
11 | 21.5 – 10 KeV | 6 | 26066
12 | 10 – 4.65 KeV | 40 | 12770
13 | 4.65 – 2.15 KeV | 21 | 20533
14 | 2.15 – 1 KeV | 27 | 20498
15 | 1 – 0.465 KeV | 20 | 13767
16 | 465 – 215 eV | 25 | 19533
17 | 215 – 100 eV | 20 | 26183
18 | 100 – 46.5 eV | 19 | 34874
19 | 46.5 – 21.5 eV | 24 | 45327
20 | 21.5 – 10 eV | 15 | 53449
21 | 10 – 4.65 eV | 17 | 58778
22 | 4.65 – 2.15 eV | 8 | 56613
23 | 2.15 – 1.0 eV | 3 | 43979
24 | 1.0 – 0.465 eV | 2 | 25874
25 | 0.465 – 0.215 eV | 1 | 10398
26 | 0.215 – 0.001 eV | 0 | 2794
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 0 | 0 | 0 | 0 | 0 | 0 | 6 | 39 | 92 | 134 | 97 | 53 | 6 | 40 | 21 | 27 | 20 | 25 | 20 | 19 | 24 | 15 | 17 | 8 | 3 | 2 | 1 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 252935 | 50467 | 30104 | 39034 | 31327 | 19175 | 10748 | 22076 | 25809 | 40473 | 47003 | 49961 | 26066 | 12770 | 20533 | 20498 | 13767 | 19533 | 26183 | 34874 | 45327 | 53449 | 58778 | 56613 | 43979 | 25874 | 10398 | 2794

## Slide 34: Sphere of Nickel Ninat R= 120 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 0 | 252911
0 | 14.0-10.5 MeV | 0 | 50480
1 | 10.5 – 6.5 MeV | 0 | 30097
2 | 6.5 – 4.0 MeV | 0 | 39041
3 | 4.0 – 2.5 MeV | 0 | 31330
4 | 2.5 – 1.4 MeV | 0 | 19170
5 | 1.4 – 0.8 MeV | 0 | 10752
6 | 0.8 – 0.4 MeV | 2 | 22062
7 | 0.4 – 0.2 MeV | 2 | 25820
8 | 0.2 – 0.1 MeV | 6 | 40494
9 | 100 – 46.5 KeV | 8 | 47032
10 | 46.5 – 21.5 KeV | 1 | 50005
11 | 21.5 – 10 KeV | 0 | 26084
12 | 10 – 4.65 KeV | 3 | 12772
13 | 4.65 – 2.15 KeV | 0 | 20536
14 | 2.15 – 1 KeV | 0 | 20522
15 | 1 – 0.465 KeV | 1 | 13781
16 | 465 – 215 eV | 1 | 19544
17 | 215 – 100 eV | 0 | 26215
18 | 100 – 46.5 eV | 3 | 34915
19 | 46.5 – 21.5 eV | 1 | 45395
20 | 21.5 – 10 eV | 0 | 53518
21 | 10 – 4.65 eV | 3 | 58847
22 | 4.65 – 2.15 eV | 0 | 56706
23 | 2.15 – 1.0 eV | 0 | 44041
24 | 1.0 – 0.465 eV | 0 | 25926
25 | 0.465 – 0.215 eV | 0 | 10412
26 | 0.215 – 0.001 eV | 0 | 2797
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 2 | 6 | 8 | 1 | 0 | 3 | 0 | 0 | 1 | 1 | 0 | 3 | 1 | 0 | 3 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 252911 | 50480 | 30097 | 39041 | 31330 | 19170 | 10752 | 22062 | 25820 | 40494 | 47032 | 50005 | 26084 | 12772 | 20536 | 20522 | 13781 | 19544 | 26215 | 34915 | 45395 | 53518 | 58847 | 56706 | 44041 | 25926 | 10412 | 2797

## Slide 35: Spectrums in metal Nickel (p=8.90 g/cm3) Ninat spheres
ABBN-78 Group № | Energy Interval | R = 1 cm |  | R = 5 cm |  | R = 10 cm |  | R = 15 cm |  | R = 20 cm |  | R = 25 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 855171 | 38129 | 450166 | 142319 | 194766 | 206527 | 81574 | 233769 | 33423 | 244697 | 13413 | 250264
0 | 14.0-10.5 MeV | 14702 | 502 | 42000 | 9147 | 41196 | 23213 | 28894 | 34452 | 17527 | 41597 | 9806 | 45677
1 | 10.5-6.5 MeV | 12915 | 531 | 27704 | 7996 | 20216 | 17815 | 10797 | 24270 | 5292 | 27506 | 2457 | 28865
2 | 6.5-4.0 MeV | 22591 | 647 | 50266 | 10105 | 35792 | 23643 | 19060 | 30944 | 9147 | 35056 | 4064 | 37242
3 | 4.0-2.5 MeV | 25269 | 334 | 69927 | 5872 | 60063 | 15499 | 36823 | 22946 | 19677 | 27119 | 9437 | 29315
4 | 2.5-1.4 MeV | 21138 | 81 | 84013 | 1806 | 101659 | 6164 | 82094 | 10911 | 53721 | 14641 | 32203 | 16570
5 | 1.4-0.8 MeV | 12632 | 77 | 73447 | 365 | 129886 | 1747 | 141048 | 4079 | 118846 | 6247 | 86346 | 7728
6 | 0.8-0.4 MeV | 5956 | 0 | 46477 | 212 | 110650 | 1397 | 160519 | 3982 | 179442 | 7653 | 166124 | 11458
7 | 0.4-0.2 MeV | 2430 | 3 | 19851 | 154 | 45453 | 998 | 66310 | 3075 | 79291 | 6149 | 81613 | 10096
8 | 0.2-0.1 MeV | 283 | 0 | 6586 | 82 | 22918 | 882 | 40876 | 3356 | 53821 | 7747 | 58290 | 13223
9 | 100-46.5 KeV | 96 | 0 | 1998 | 54 | 7540 | 578 | 16249 | 2643 | 24119 | 6884 | 28469 | 13221
10 | 46.5 –21.5 KeV | 0 | 0 | 353 | 12 | 2453 | 370 | 6150 | 2030 | 10111 | 6038 | 12768 | 12073
11 | 21.5– 10 KeV | 0 | 0 | 9 | 4 | 145 | 151 | 523 | 939 | 893 | 2931 | 1217 | 6086
12 | 10– 4.65 KeV | 0 | 0 | 39 | 0 | 758 | 53 | 2619 | 414 | 4814 | 1316 | 6323 | 2820
13 | 4.65– 2.15 KeV | 0 | 0 | 7 | 0 | 308 | 55 | 1203 | 557 | 2363 | 1954 | 3103 | 4229
14 | 2.15 – 1 KeV | 0 | 0 | 1 | 0 | 327 | 60 | 1355 | 509 | 2840 | 1809 | 4033 | 4199
15 | 1– 0.465 KeV | 0 | 0 | 0 | 0 | 198 | 31 | 1119 | 322 | 2333 | 1178 | 3399 | 2697
16 | 465– 215 eV | 0 | 0 | 2 | 0 | 118 | 24 | 956 | 366 | 2118 | 1528 | 3016 | 3720
17 | 215– 100 eV | 0 | 0 | 1 | 0 | 86 | 31 | 730 | 424 | 1789 | 1886 | 2555 | 4639
18 | 100– 46.5 eV | 0 | 0 | 2 | 0 | 70 | 33 | 597 | 531 | 1507 | 2448 | 2333 | 5930
19 | 46.5– 21.5 eV | 0 | 0 | 0 | 0 | 40 | 23 | 437 | 588 | 1240 | 2837 | 1925 | 7285
20 | 21.5– 10 eV | 0 | 0 | 0 | 0 | 31 | 36 | 304 | 671 | 952 | 3132 | 1519 | 8389
21 | 10– 4.65 eV | 0 | 0 | 0 | 0 | 16 | 29 | 215 | 616 | 637 | 3166 | 1071 | 8771
22 | 4.6 – 2.15 eV | 0 | 0 | 0 | 0 | 2 | 12 | 128 | 507 | 414 | 2833 | 634 | 8084
23 | 2.1 – 1.0 eV | 0 | 0 | 0 | 0 | 3 | 10 | 51 | 382 | 182 | 2142 | 335 | 6033
24 | 1.0– 0.465 eV | 0 | 0 | 0 | 0 | 1 | 7 | 15 | 205 | 59 | 1169 | 144 | 3301
25 | 0.46 – 0.215 eV | 0 | 0 | 0 | 0 | 0 | 0 | 3 | 90 | 17 | 421 | 43 | 1262
26 | 0.215– 0.001 eV | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 9 | 0 | 98 | 2 | 335
Average Neutron Energy |  | 12.89 MeV | 13.74 MeV | 9.02 MeV | 12.74 MeV | 5.48 MeV | 11.85 MeV | 3.23 MeV | 10.97 MeV | 1.94 MeV | 9.80 MeV | 1.24 MeV | 8.49 MeV
Diffusion/Absorption time of spectra, nanoseconds |  | 0.232 | 0.100 | 2.48 | 0.596 | 13.54 | 6.93 | 54.61 | 122.02 | 134.09 | 525.48 | 232.09 | 1221
Number of neutrons |  | 973183 | 40234 | 872849 | 178128 | 774695 | 299388 | 700649 | 383587 | 626575 | 462182 | 536642 | 553512

## Slide 36: Spectrums in metal Nickel (p=8.90 g/cm3) Ninat spheres
ABBN-78 Group № | Energy Interval | R = 30 cm |  | R = 40 cm |  | R = 65 cm |  | R = 80 cm |  | R = 100 cm |  | R = 120 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 5306 | 251973 | 799 | 252566 | 6 | 253196 | 1 | 253034 | 0 | 252935 | 0 | 252911
0 | 14.0-10.5 MeV | 5146 | 48052 | 1213 | 49787 | 29 | 50393 | 4 | 50438 | 0 | 50467 | 0 | 50480
1 | 10.5-6.5 MeV | 1104 | 29602 | 209 | 30040 | 3 | 30189 | 0 | 30051 | 0 | 30104 | 0 | 30097
2 | 6.5-4.0 MeV | 1817 | 38148 | 324 | 38788 | 2 | 38985 | 0 | 39086 | 0 | 39034 | 0 | 39041
3 | 4.0-2.5 MeV | 4495 | 30139 | 915 | 31372 | 14 | 31417 | 0 | 31349 | 0 | 31327 | 0 | 31330
4 | 2.5-1.4 MeV | 17685 | 17913 | 4701 | 18989 | 123 | 19255 | 10 | 19194 | 0 | 19175 | 0 | 19170
5 | 1.4-0.8 MeV | 56539 | 8912 | 20074 | 10218 | 772 | 10702 | 103 | 10713 | 6 | 10748 | 0 | 10752
6 | 0.8-0.4 MeV | 134926 | 14768 | 69853 | 19169 | 5568 | 21914 | 887 | 22004 | 39 | 22076 | 2 | 22062
7 | 0.4-0.2 MeV | 75659 | 13869 | 49006 | 20120 | 6073 | 25355 | 1169 | 25733 | 92 | 25809 | 2 | 25820
8 | 0.2-0.1 MeV | 56635 | 19321 | 40244 | 29705 | 6539 | 39331 | 1410 | 40306 | 134 | 40473 | 6 | 40494
9 | 100-46.5 KeV | 28717 | 20097 | 22190 | 32125 | 4206 | 45299 | 977 | 46729 | 97 | 47003 | 8 | 47032
10 | 46.5 –21.5 KeV | 13647 | 19288 | 10850 | 32815 | 2189 | 47991 | 552 | 49568 | 53 | 49961 | 1 | 50005
11 | 21.5– 10 KeV | 1213 | 9672 | 1035 | 16903 | 212 | 25062 | 55 | 25866 | 6 | 26066 | 0 | 26084
12 | 10– 4.65 KeV | 7013 | 4653 | 5850 | 8137 | 1233 | 12191 | 327 | 12664 | 40 | 12770 | 3 | 12772
13 | 4.65– 2.15 KeV | 3555 | 7049 | 2983 | 12852 | 668 | 19555 | 170 | 20371 | 21 | 20533 | 0 | 20536
14 | 2.15 – 1 KeV | 4538 | 6951 | 3810 | 12628 | 867 | 19547 | 236 | 20305 | 27 | 20498 | 0 | 20522
15 | 1– 0.465 KeV | 3772 | 4566 | 3406 | 8510 | 755 | 13159 | 196 | 13620 | 20 | 13767 | 1 | 13781
16 | 465– 215 eV | 3624 | 6414 | 3185 | 11829 | 785 | 18567 | 222 | 19339 | 25 | 19533 | 1 | 19544
17 | 215– 100 eV | 3290 | 8103 | 2973 | 15684 | 673 | 24973 | 196 | 25919 | 20 | 26183 | 0 | 26215
18 | 100– 46.5 eV | 2820 | 10719 | 2662 | 20328 | 673 | 32842 | 155 | 34524 | 19 | 34874 | 3 | 34915
19 | 46.5– 21.5 eV | 2409 | 13509 | 2335 | 25891 | 571 | 42489 | 173 | 44763 | 24 | 45327 | 1 | 45395
20 | 21.5– 10 eV | 1840 | 15621 | 1842 | 30492 | 498 | 50069 | 132 | 52770 | 15 | 53449 | 0 | 53518
21 | 10– 4.65 eV | 1400 | 16368 | 1361 | 32755 | 349 | 55013 | 93 | 58062 | 17 | 58778 | 3 | 58847
22 | 4.6 – 2.15 eV | 875 | 15075 | 837 | 31212 | 234 | 52935 | 67 | 55854 | 8 | 56613 | 0 | 56706
23 | 2.1 – 1.0 eV | 433 | 11614 | 461 | 24105 | 133 | 41259 | 32 | 43392 | 3 | 43979 | 0 | 44041
24 | 1.0– 0.465 eV | 171 | 6721 | 171 | 13928 | 54 | 24156 | 11 | 25499 | 2 | 25874 | 0 | 25926
25 | 0.46 – 0.215 eV | 36 | 2596 | 44 | 5444 | 9 | 9651 | 2 | 10241 | 1 | 10398 | 0 | 10412
26 | 0.215– 0.001 eV | 5 | 637 | 3 | 1409 | 2 | 2604 | 0 | 2757 | 0 | 2794 | 0 | 2797
Average Neutron Energy |  | 855 KeV | 7.32 MeV | 484 KeV | 5.76 MeV | 224 KeV | 4.59 MeV | 175 KeV | 4.47 MeV | 116 KeV | 4.45 MeV | 94.96 KeV | 4.44 MeV
Diffusion/Absorption time of spectra, nanoseconds |  | 337.22 | 1985 | 536.87 | 3161 | 996.84 | 4269 | 1206 | 4395 | 1649 | 4429 | 1878 | 4433
Number of neutrons |  | 438670 | 652350 | 253336 | 837801 | 33240 | 1058099 | 7180 | 1084151 | 669 | 1090548 | 31 | 1091205

## Slide 37: Neutron cross sections of C12 : total cross section (blue line), capture (red), inelastic scattering (green line). Data from the Brookhaven National Laboratory [5].

## Slide 38: ABBN-78 constants for C12

## Slide 39: Sphere of graphite (p=2.26 g/cm3) C12 R= 1 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 872291 | 8441
0 | 14.0-10.5 MeV | 69757 | 428
1 | 10.5 – 6.5 MeV | 20476 | 136
2 | 6.5 – 4.0 MeV | 5067 | 0
3 | 4.0 – 2.5 MeV | 4886 | 0
4 | 2.5 – 1.4 MeV | 7960 | 0
5 | 1.4 – 0.8 MeV | 5536 | 0
6 | 0.8 – 0.4 MeV | 3312 | 0
7 | 0.4 – 0.2 MeV | 1180 | 0
8 | 0.2 – 0.1 MeV | 376 | 0
9 | 100 – 46.5 KeV | 148 | 0
10 | 46.5 – 21.5 KeV | 6 | 0
11 | 21.5 – 10 KeV | 0 | 0
12 | 10 – 4.65 KeV | 0 | 0
13 | 4.65 – 2.15 KeV | 0 | 0
14 | 2.15 – 1 KeV | 0 | 0
15 | 1 – 0.465 KeV | 0 | 0
16 | 465 – 215 eV | 0 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 872291 | 69757 | 20476 | 5067 | 4886 | 7960 | 5536 | 3312 | 1180 | 376 | 148 | 6 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 8441 | 428 | 136 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 40: Sphere of graphite (p=2.26 g/cm3) C12 R= 5 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 504962 | 33060
0 | 14.0-10.5 MeV | 219675 | 8464
1 | 10.5 – 6.5 MeV | 74214 | 2655
2 | 6.5 – 4.0 MeV | 41273 | 0
3 | 4.0 – 2.5 MeV | 21492 | 0
4 | 2.5 – 1.4 MeV | 37456 | 0
5 | 1.4 – 0.8 MeV | 25204 | 0
6 | 0.8 – 0.4 MeV | 17174 | 0
7 | 0.4 – 0.2 MeV | 7996 | 0
8 | 0.2 – 0.1 MeV | 3704 | 0
9 | 100 – 46.5 KeV | 1693 | 0
10 | 46.5 – 21.5 KeV | 623 | 0
11 | 21.5 – 10 KeV | 238 | 0
12 | 10 – 4.65 KeV | 76 | 0
13 | 4.65 – 2.15 KeV | 20 | 0
14 | 2.15 – 1 KeV | 14 | 0
15 | 1 – 0.465 KeV | 6 | 0
16 | 465 – 215 eV | 1 | 0
17 | 215 – 100 eV | 0 | 0
18 | 100 – 46.5 eV | 0 | 0
19 | 46.5 – 21.5 eV | 0 | 0
20 | 21.5 – 10 eV | 0 | 0
21 | 10 – 4.65 eV | 0 | 0
22 | 4.65 – 2.15 eV | 0 | 0
23 | 2.15 – 1.0 eV | 0 | 0
24 | 1.0 – 0.465 eV | 0 | 0
25 | 0.465 – 0.215 eV | 0 | 0
26 | 0.215 – 0.001 eV | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 504962 | 219675 | 74214 | 41273 | 21492 | 37456 | 25204 | 17174 | 7996 | 3704 | 1693 | 623 | 238 | 76 | 20 | 14 | 6 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 33060 | 8464 | 2655 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0

## Slide 41: Sphere of graphite (p=2.26 g/cm3) C12 R= 10 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 254733 | 49511
0 | 14.0-10.5 MeV | 242671 | 24083
1 | 10.5 – 6.5 MeV | 99406 | 8460
2 | 6.5 – 4.0 MeV | 83829 | 0
3 | 4.0 – 2.5 MeV | 38228 | 0
4 | 2.5 – 1.4 MeV | 66182 | 0
5 | 1.4 – 0.8 MeV | 44184 | 0
6 | 0.8 – 0.4 MeV | 32629 | 0
7 | 0.4 – 0.2 MeV | 19000 | 0
8 | 0.2 – 0.1 MeV | 11957 | 0
9 | 100 – 46.5 KeV | 8471 | 0
10 | 46.5 – 21.5 KeV | 5584 | 0
11 | 21.5 – 10 KeV | 3636 | 0
12 | 10 – 4.65 KeV | 2432 | 0
13 | 4.65 – 2.15 KeV | 1608 | 0
14 | 2.15 – 1 KeV | 1116 | 0
15 | 1 – 0.465 KeV | 742 | 0
16 | 465 – 215 eV | 511 | 0
17 | 215 – 100 eV | 315 | 0
18 | 100 – 46.5 eV | 239 | 0
19 | 46.5 – 21.5 eV | 163 | 0
20 | 21.5 – 10 eV | 107 | 0
21 | 10 – 4.65 eV | 71 | 0
22 | 4.65 – 2.15 eV | 49 | 0
23 | 2.15 – 1.0 eV | 24 | 0
24 | 1.0 – 0.465 eV | 16 | 0
25 | 0.465 – 0.215 eV | 14 | 0
26 | 0.215 – 0.001 eV | 28 | 1
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 254733 | 242671 | 99406 | 83829 | 38228 | 66182 | 44184 | 32629 | 19000 | 11957 | 8471 | 5584 | 3636 | 2432 | 1608 | 1116 | 742 | 511 | 315 | 239 | 163 | 107 | 71 | 49 | 24 | 16 | 14 | 28
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 49511 | 24083 | 8460 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1

## Slide 42: Sphere of graphite (p=2.26 g/cm3) C12 R= 15 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 129018 | 58304
0 | 14.0-10.5 MeV | 196308 | 38736
1 | 10.5 – 6.5 MeV | 97619 | 15294
2 | 6.5 – 4.0 MeV | 101929 | 0
3 | 4.0 – 2.5 MeV | 47005 | 0
4 | 2.5 – 1.4 MeV | 81702 | 0
5 | 1.4 – 0.8 MeV | 56003 | 0
6 | 0.8 – 0.4 MeV | 43343 | 0
7 | 0.4 – 0.2 MeV | 27642 | 0
8 | 0.2 – 0.1 MeV | 19820 | 0
9 | 100 – 46.5 KeV | 16797 | 0
10 | 46.5 – 21.5 KeV | 13022 | 0
11 | 21.5 – 10 KeV | 10461 | 0
12 | 10 – 4.65 KeV | 8613 | 0
13 | 4.65 – 2.15 KeV | 7074 | 0
14 | 2.15 – 1 KeV | 5817 | 0
15 | 1 – 0.465 KeV | 4792 | 1
16 | 465 – 215 eV | 3820 | 2
17 | 215 – 100 eV | 3106 | 0
18 | 100 – 46.5 eV | 2523 | 0
19 | 46.5 – 21.5 eV | 2022 | 0
20 | 21.5 – 10 eV | 1685 | 0
21 | 10 – 4.65 eV | 1393 | 1
22 | 4.65 – 2.15 eV | 1131 | 1
23 | 2.15 – 1.0 eV | 909 | 1
24 | 1.0 – 0.465 eV | 759 | 4
25 | 0.465 – 0.215 eV | 620 | 2
26 | 0.215 – 0.001 eV | 2674 | 47
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 129018 | 196308 | 97619 | 101929 | 47005 | 81702 | 56003 | 43343 | 27642 | 19820 | 16797 | 13022 | 10461 | 8613 | 7074 | 5817 | 4792 | 3820 | 3106 | 2523 | 2022 | 1685 | 1393 | 1131 | 909 | 759 | 620 | 2674
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 58304 | 38736 | 15294 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 2 | 0 | 0 | 0 | 0 | 1 | 1 | 1 | 4 | 2 | 47

## Slide 43: Sphere of graphite (p=2.26 g/cm3) C12 R= 20 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 64846 | 63008
0 | 14.0-10.5 MeV | 140756 | 50282
1 | 10.5 – 6.5 MeV | 83333 | 21714
2 | 6.5 – 4.0 MeV | 97411 | 0
3 | 4.0 – 2.5 MeV | 47257 | 0
4 | 2.5 – 1.4 MeV | 84329 | 0
5 | 1.4 – 0.8 MeV | 58673 | 0
6 | 0.8 – 0.4 MeV | 46944 | 0
7 | 0.4 – 0.2 MeV | 31500 | 0
8 | 0.2 – 0.1 MeV | 23803 | 0
9 | 100 – 46.5 KeV | 21608 | 0
10 | 46.5 – 21.5 KeV | 18508 | 0
11 | 21.5 – 10 KeV | 16155 | 0
12 | 10 – 4.65 KeV | 14505 | 0
13 | 4.65 – 2.15 KeV | 12970 | 0
14 | 2.15 – 1 KeV | 11769 | 0
15 | 1 – 0.465 KeV | 10578 | 2
16 | 465 – 215 eV | 9192 | 1
17 | 215 – 100 eV | 8063 | 3
18 | 100 – 46.5 eV | 7148 | 4
19 | 46.5 – 21.5 eV | 6506 | 5
20 | 21.5 – 10 eV | 5634 | 6
21 | 10 – 4.65 eV | 4946 | 6
22 | 4.65 – 2.15 eV | 4386 | 14
23 | 2.15 – 1.0 eV | 3907 | 26
24 | 1.0 – 0.465 eV | 3400 | 19
25 | 0.465 – 0.215 eV | 3156 | 26
26 | 0.215 – 0.001 eV | 22939 | 662
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 64846 | 140756 | 83333 | 97411 | 47257 | 84329 | 58673 | 46944 | 31500 | 23803 | 21608 | 18508 | 16155 | 14505 | 12970 | 11769 | 10578 | 9192 | 8063 | 7148 | 6506 | 5634 | 4946 | 4386 | 3907 | 3400 | 3156 | 22939
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 63008 | 50282 | 21714 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 1 | 3 | 4 | 5 | 6 | 6 | 14 | 26 | 19 | 26 | 662

## Slide 44: Sphere of graphite (p=2.26 g/cm3) C12 R= 25 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 32711 | 64496
0 | 14.0-10.5 MeV | 93513 | 58606
1 | 10.5 – 6.5 MeV | 66047 | 26845
2 | 6.5 – 4.0 MeV | 82755 | 0
3 | 4.0 – 2.5 MeV | 41872 | 0
4 | 2.5 – 1.4 MeV | 76360 | 0
5 | 1.4 – 0.8 MeV | 54136 | 0
6 | 0.8 – 0.4 MeV | 44416 | 0
7 | 0.4 – 0.2 MeV | 30621 | 0
8 | 0.2 – 0.1 MeV | 24183 | 0
9 | 100 – 46.5 KeV | 22715 | 0
10 | 46.5 – 21.5 KeV | 20243 | 0
11 | 21.5 – 10 KeV | 18614 | 0
12 | 10 – 4.65 KeV | 17497 | 0
13 | 4.65 – 2.15 KeV | 16301 | 0
14 | 2.15 – 1 KeV | 15226 | 2
15 | 1 – 0.465 KeV | 14201 | 3
16 | 465 – 215 eV | 13467 | 4
17 | 215 – 100 eV | 12691 | 6
18 | 100 – 46.5 eV | 11686 | 11
19 | 46.5 – 21.5 eV | 10940 | 15
20 | 21.5 – 10 eV | 9972 | 16
21 | 10 – 4.65 eV | 9159 | 23
22 | 4.65 – 2.15 eV | 8777 | 34
23 | 2.15 – 1.0 eV | 7909 | 39
24 | 1.0 – 0.465 eV | 7392 | 68
25 | 0.465 – 0.215 eV | 6938 | 80
26 | 0.215 – 0.001 eV | 76253 | 3157
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 32711 | 93513 | 66047 | 82755 | 41872 | 76360 | 54136 | 44416 | 30621 | 24183 | 22715 | 20243 | 18614 | 17497 | 16301 | 15226 | 14201 | 13467 | 12691 | 11686 | 10940 | 9972 | 9159 | 8777 | 7909 | 7392 | 6938 | 76253
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 64496 | 58606 | 26845 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 3 | 4 | 6 | 11 | 15 | 16 | 23 | 34 | 39 | 68 | 80 | 3157

## Slide 45: Sphere of graphite (p=2.26 g/cm3) C12 R= 30 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 16278 | 65504
0 | 14.0-10.5 MeV | 59089 | 63680
1 | 10.5 – 6.5 MeV | 48647 | 30720
2 | 6.5 – 4.0 MeV | 64849 | 0
3 | 4.0 – 2.5 MeV | 34028 | 0
4 | 2.5 – 1.4 MeV | 63188 | 0
5 | 1.4 – 0.8 MeV | 46285 | 0
6 | 0.8 – 0.4 MeV | 38548 | 0
7 | 0.4 – 0.2 MeV | 27491 | 0
8 | 0.2 – 0.1 MeV | 21655 | 0
9 | 100 – 46.5 KeV | 21048 | 0
10 | 46.5 – 21.5 KeV | 19422 | 0
11 | 21.5 – 10 KeV | 17730 | 0
12 | 10 – 4.65 KeV | 17125 | 0
13 | 4.65 – 2.15 KeV | 16894 | 0
14 | 2.15 – 1 KeV | 16186 | 2
15 | 1 – 0.465 KeV | 15899 | 2
16 | 465 – 215 eV | 15526 | 12
17 | 215 – 100 eV | 14750 | 12
18 | 100 – 46.5 eV | 14030 | 24
19 | 46.5 – 21.5 eV | 13364 | 23
20 | 21.5 – 10 eV | 12929 | 28
21 | 10 – 4.65 eV | 12307 | 46
22 | 4.65 – 2.15 eV | 11799 | 78
23 | 2.15 – 1.0 eV | 11238 | 88
24 | 1.0 – 0.465 eV | 10445 | 117
25 | 0.465 – 0.215 eV | 10026 | 141
26 | 0.215 – 0.001 eV | 159154 | 9593
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 16278 | 59089 | 48647 | 64849 | 34028 | 63188 | 46285 | 38548 | 27491 | 21655 | 21048 | 19422 | 17730 | 17125 | 16894 | 16186 | 15899 | 15526 | 14750 | 14030 | 13364 | 12929 | 12307 | 11799 | 11238 | 10445 | 10026 | 159154
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 65504 | 63680 | 30720 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 2 | 2 | 12 | 12 | 24 | 23 | 28 | 46 | 78 | 88 | 117 | 141 | 9593

## Slide 46: Sphere of graphite (p=2.26 g/cm3) C12 R= 40 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 4167 | 66796
0 | 14.0-10.5 MeV | 21384 | 69082
1 | 10.5 – 6.5 MeV | 23925 | 35723
2 | 6.5 – 4.0 MeV | 33686 | 0
3 | 4.0 – 2.5 MeV | 18747 | 0
4 | 2.5 – 1.4 MeV | 37010 | 0
5 | 1.4 – 0.8 MeV | 28040 | 0
6 | 0.8 – 0.4 MeV | 23844 | 0
7 | 0.4 – 0.2 MeV | 17488 | 0
8 | 0.2 – 0.1 MeV | 14324 | 0
9 | 100 – 46.5 KeV | 14215 | 0
10 | 46.5 – 21.5 KeV | 13335 | 0
11 | 21.5 – 10 KeV | 12868 | 0
12 | 10 – 4.65 KeV | 12854 | 0
13 | 4.65 – 2.15 KeV | 13021 | 0
14 | 2.15 – 1 KeV | 12946 | 4
15 | 1 – 0.465 KeV | 12866 | 11
16 | 465 – 215 eV | 12901 | 22
17 | 215 – 100 eV | 12687 | 23
18 | 100 – 46.5 eV | 12841 | 31
19 | 46.5 – 21.5 eV | 12727 | 49
20 | 21.5 – 10 eV | 12593 | 65
21 | 10 – 4.65 eV | 12524 | 96
22 | 4.65 – 2.15 eV | 12460 | 138
23 | 2.15 – 1.0 eV | 12069 | 191
24 | 1.0 – 0.465 eV | 11893 | 263
25 | 0.465 – 0.215 eV | 11894 | 372
26 | 0.215 – 0.001 eV | 350289 | 37536
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 4167 | 21384 | 23925 | 33686 | 18747 | 37010 | 28040 | 23844 | 17488 | 14324 | 14215 | 13335 | 12868 | 12854 | 13021 | 12946 | 12866 | 12901 | 12687 | 12841 | 12727 | 12593 | 12524 | 12460 | 12069 | 11893 | 11894 | 350289
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 66796 | 69082 | 35723 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4 | 11 | 22 | 23 | 31 | 49 | 65 | 96 | 138 | 191 | 263 | 372 | 37536

## Slide 47: Sphere of graphite (p=2.26 g/cm3) C12 R= 50 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 1020 | 67220
0 | 14.0-10.5 MeV | 7209 | 70661
1 | 10.5 – 6.5 MeV | 10346 | 37775
2 | 6.5 – 4.0 MeV | 15545 | 0
3 | 4.0 – 2.5 MeV | 8942 | 0
4 | 2.5 – 1.4 MeV | 18803 | 0
5 | 1.4 – 0.8 MeV | 14393 | 0
6 | 0.8 – 0.4 MeV | 12629 | 0
7 | 0.4 – 0.2 MeV | 9547 | 0
8 | 0.2 – 0.1 MeV | 7922 | 0
9 | 100 – 46.5 KeV | 7744 | 0
10 | 46.5 – 21.5 KeV | 7395 | 0
11 | 21.5 – 10 KeV | 7331 | 0
12 | 10 – 4.65 KeV | 7256 | 0
13 | 4.65 – 2.15 KeV | 7702 | 0
14 | 2.15 – 1 KeV | 7799 | 9
15 | 1 – 0.465 KeV | 7909 | 12
16 | 465 – 215 eV | 8048 | 20
17 | 215 – 100 eV | 8270 | 12
18 | 100 – 46.5 eV | 8476 | 30
19 | 46.5 – 21.5 eV | 8819 | 68
20 | 21.5 – 10 eV | 8639 | 97
21 | 10 – 4.65 eV | 8781 | 142
22 | 4.65 – 2.15 eV | 9137 | 181
23 | 2.15 – 1.0 eV | 9040 | 251
24 | 1.0 – 0.465 eV | 9218 | 399
25 | 0.465 – 0.215 eV | 9291 | 593
26 | 0.215 – 0.001 eV | 491072 | 84247
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 1020 | 7209 | 10346 | 15545 | 8942 | 18803 | 14393 | 12629 | 9547 | 7922 | 7744 | 7395 | 7331 | 7256 | 7702 | 7799 | 7909 | 8048 | 8270 | 8476 | 8819 | 8639 | 8781 | 9137 | 9040 | 9218 | 9291 | 491072
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 67220 | 70661 | 37775 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 9 | 12 | 20 | 12 | 30 | 68 | 97 | 142 | 181 | 251 | 399 | 593 | 84247

## Slide 48: Sphere of graphite (p=2.26 g/cm3) C12 R= 65 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 129 | 67269
0 | 14.0-10.5 MeV | 1296 | 71634
1 | 10.5 – 6.5 MeV | 2669 | 38939
2 | 6.5 – 4.0 MeV | 4065 | 0
3 | 4.0 – 2.5 MeV | 2555 | 0
4 | 2.5 – 1.4 MeV | 5503 | 0
5 | 1.4 – 0.8 MeV | 4501 | 0
6 | 0.8 – 0.4 MeV | 3977 | 0
7 | 0.4 – 0.2 MeV | 3078 | 0
8 | 0.2 – 0.1 MeV | 2582 | 0
9 | 100 – 46.5 KeV | 2649 | 0
10 | 46.5 – 21.5 KeV | 2552 | 0
11 | 21.5 – 10 KeV | 2531 | 0
12 | 10 – 4.65 KeV | 2741 | 0
13 | 4.65 – 2.15 KeV | 2727 | 0
14 | 2.15 – 1 KeV | 2796 | 5
15 | 1 – 0.465 KeV | 3014 | 20
16 | 465 – 215 eV | 3074 | 21
17 | 215 – 100 eV | 3091 | 31
18 | 100 – 46.5 eV | 3156 | 46
19 | 46.5 – 21.5 eV | 3462 | 79
20 | 21.5 – 10 eV | 3509 | 121
21 | 10 – 4.65 eV | 3592 | 157
22 | 4.65 – 2.15 eV | 3769 | 259
23 | 2.15 – 1.0 eV | 3855 | 308
24 | 1.0 – 0.465 eV | 3979 | 454
25 | 0.465 – 0.215 eV | 4233 | 727
26 | 0.215 – 0.001 eV | 557249 | 177596
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 129 | 1296 | 2669 | 4065 | 2555 | 5503 | 4501 | 3977 | 3078 | 2582 | 2649 | 2552 | 2531 | 2741 | 2727 | 2796 | 3014 | 3074 | 3091 | 3156 | 3462 | 3509 | 3592 | 3769 | 3855 | 3979 | 4233 | 557249
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 67269 | 71634 | 38939 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 5 | 20 | 21 | 31 | 46 | 79 | 121 | 157 | 259 | 308 | 454 | 727 | 177596

## Slide 49: Sphere of graphite (p=2.26 g/cm3) C12 R= 80 cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 17 | 66876
0 | 14.0-10.5 MeV | 183 | 71870
1 | 10.5 – 6.5 MeV | 643 | 39304
2 | 6.5 – 4.0 MeV | 1030 | 0
3 | 4.0 – 2.5 MeV | 621 | 0
4 | 2.5 – 1.4 MeV | 1364 | 0
5 | 1.4 – 0.8 MeV | 1150 | 0
6 | 0.8 – 0.4 MeV | 1038 | 0
7 | 0.4 – 0.2 MeV | 807 | 0
8 | 0.2 – 0.1 MeV | 725 | 0
9 | 100 – 46.5 KeV | 749 | 0
10 | 46.5 – 21.5 KeV | 691 | 0
11 | 21.5 – 10 KeV | 768 | 0
12 | 10 – 4.65 KeV | 749 | 0
13 | 4.65 – 2.15 KeV | 834 | 0
14 | 2.15 – 1 KeV | 820 | 10
15 | 1 – 0.465 KeV | 879 | 16
16 | 465 – 215 eV | 910 | 26
17 | 215 – 100 eV | 1019 | 38
18 | 100 – 46.5 eV | 1024 | 57
19 | 46.5 – 21.5 eV | 1074 | 78
20 | 21.5 – 10 eV | 1106 | 130
21 | 10 – 4.65 eV | 1147 | 187
22 | 4.65 – 2.15 eV | 1312 | 275
23 | 2.15 – 1.0 eV | 1233 | 367
24 | 1.0 – 0.465 eV | 1289 | 565
25 | 0.465 – 0.215 eV | 1434 | 805
26 | 0.215 – 0.001 eV | 513917 | 280863
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 17 | 183 | 643 | 1030 | 621 | 1364 | 1150 | 1038 | 807 | 725 | 749 | 691 | 768 | 749 | 834 | 820 | 879 | 910 | 1019 | 1024 | 1074 | 1106 | 1147 | 1312 | 1233 | 1289 | 1434 | 513917
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 66876 | 71870 | 39304 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 10 | 16 | 26 | 38 | 57 | 78 | 130 | 187 | 275 | 367 | 565 | 805 | 280863

## Slide 50: Sphere of graphite (p=2.26 g/cm3) C12 R= 100cm Outgoing spectrum (upper picture, blue curve) and capture spectrum (picture below, red line).
ABBN-78 Group № | Energy interval | Outgoing spectrum | Capture spectrum
-1 | 14.5-14.0 MeV | 0 | 67073
0 | 14.0-10.5 MeV | 15 | 71857
1 | 10.5 – 6.5 MeV | 79 | 39486
2 | 6.5 – 4.0 MeV | 122 | 0
3 | 4.0 – 2.5 MeV | 72 | 0
4 | 2.5 – 1.4 MeV | 195 | 0
5 | 1.4 – 0.8 MeV | 153 | 0
6 | 0.8 – 0.4 MeV | 124 | 0
7 | 0.4 – 0.2 MeV | 115 | 0
8 | 0.2 – 0.1 MeV | 95 | 0
9 | 100 – 46.5 KeV | 115 | 0
10 | 46.5 – 21.5 KeV | 111 | 0
11 | 21.5 – 10 KeV | 98 | 0
12 | 10 – 4.65 KeV | 110 | 0
13 | 4.65 – 2.15 KeV | 124 | 0
14 | 2.15 – 1 KeV | 133 | 10
15 | 1 – 0.465 KeV | 150 | 13
16 | 465 – 215 eV | 144 | 25
17 | 215 – 100 eV | 150 | 41
18 | 100 – 46.5 eV | 175 | 51
19 | 46.5 – 21.5 eV | 191 | 77
20 | 21.5 – 10 eV | 183 | 133
21 | 10 – 4.65 eV | 221 | 188
22 | 4.65 – 2.15 eV | 220 | 265
23 | 2.15 – 1.0 eV | 217 | 359
24 | 1.0 – 0.465 eV | 266 | 560
25 | 0.465 – 0.215 eV | 257 | 820
26 | 0.215 – 0.001 eV | 409606 | 590394
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 0 | 15 | 79 | 122 | 72 | 195 | 153 | 124 | 115 | 95 | 115 | 111 | 98 | 110 | 124 | 133 | 150 | 144 | 150 | 175 | 191 | 183 | 221 | 220 | 217 | 266 | 257 | 409606
Chart: 
| -1 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26
 | 67073 | 71857 | 39486 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 10 | 13 | 25 | 41 | 51 | 77 | 133 | 188 | 265 | 359 | 560 | 820 | 590394

## Slide 51: Spectrums in graphite (p=2.26 g/cm3) C12 spheres
ABBN-78 Group № | Energy Interval | R = 1 cm |  | R = 5 cm |  | R = 10 cm |  | R = 15 cm |  | R = 20 cm |  | R = 25 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 872291 | 8441 | 504962 | 33060 | 254733 | 49511 | 129018 | 58304 | 64846 | 63008 | 32711 | 64496
0 | 14.0-10.5 MeV | 69757 | 428 | 219675 | 8464 | 242671 | 24083 | 196308 | 38736 | 140756 | 50282 | 93513 | 58606
1 | 10.5-6.5 MeV | 20476 | 136 | 74214 | 2655 | 99406 | 8460 | 97619 | 15294 | 83333 | 21714 | 66047 | 26845
2 | 6.5-4.0 MeV | 5067 | 0 | 41273 | 0 | 83829 | 0 | 101929 | 0 | 97411 | 0 | 82755 | 0
3 | 4.0-2.5 MeV | 4886 | 0 | 21492 | 0 | 38228 | 0 | 47005 | 0 | 47257 | 0 | 41872 | 0
4 | 2.5-1.4 MeV | 7960 | 0 | 37456 | 0 | 66182 | 0 | 81702 | 0 | 84329 | 0 | 76360 | 0
5 | 1.4-0.8 MeV | 5536 | 0 | 25204 | 0 | 44184 | 0 | 56003 | 0 | 58673 | 0 | 54136 | 0
6 | 0.8-0.4 MeV | 3312 | 0 | 17174 | 0 | 32629 | 0 | 43343 | 0 | 46944 | 0 | 44416 | 0
7 | 0.4-0.2 MeV | 1180 | 0 | 7996 | 0 | 19000 | 0 | 27642 | 0 | 31500 | 0 | 30621 | 0
8 | 0.2-0.1 MeV | 376 | 0 | 3704 | 0 | 11957 | 0 | 19820 | 0 | 23803 | 0 | 24183 | 0
9 | 100-46.5 KeV | 148 | 0 | 1693 | 0 | 8471 | 0 | 16797 | 0 | 21608 | 0 | 22715 | 0
10 | 46.5 –21.5 KeV | 6 | 0 | 623 | 0 | 5584 | 0 | 13022 | 0 | 18508 | 0 | 20243 | 0
11 | 21.5– 10 KeV | 0 | 0 | 238 | 0 | 3636 | 0 | 10461 | 0 | 16155 | 0 | 18614 | 0
12 | 10– 4.65 KeV | 0 | 0 | 76 | 0 | 2432 | 0 | 8613 | 0 | 14505 | 0 | 17497 | 0
13 | 4.65– 2.15 KeV | 0 | 0 | 20 | 0 | 1608 | 0 | 7074 | 0 | 12970 | 0 | 16301 | 0
14 | 2.15 – 1 KeV | 0 | 0 | 14 | 0 | 1116 | 0 | 5817 | 0 | 11769 | 0 | 15226 | 2
15 | 1– 0.465 KeV | 0 | 0 | 6 | 0 | 742 | 0 | 4792 | 1 | 10578 | 2 | 14201 | 3
16 | 465– 215 eV | 0 | 0 | 1 | 0 | 511 | 0 | 3820 | 2 | 9192 | 1 | 13467 | 4
17 | 215– 100 eV | 0 | 0 | 0 | 0 | 315 | 0 | 3106 | 0 | 8063 | 3 | 12691 | 6
18 | 100– 46.5 eV | 0 | 0 | 0 | 0 | 239 | 0 | 2523 | 0 | 7148 | 4 | 11686 | 11
19 | 46.5– 21.5 eV | 0 | 0 | 0 | 0 | 163 | 0 | 2022 | 0 | 6506 | 5 | 10940 | 15
20 | 21.5– 10 eV | 0 | 0 | 0 | 0 | 107 | 0 | 1685 | 0 | 5634 | 6 | 9972 | 16
21 | 10– 4.65 eV | 0 | 0 | 0 | 0 | 71 | 0 | 1393 | 1 | 4946 | 6 | 9159 | 23
22 | 4.6 – 2.15 eV | 0 | 0 | 0 | 0 | 49 | 0 | 1131 | 1 | 4386 | 14 | 8777 | 34
23 | 2.1 – 1.0 eV | 0 | 0 | 0 | 0 | 24 | 0 | 909 | 1 | 3907 | 26 | 7909 | 39
24 | 1.0– 0.465 eV | 0 | 0 | 0 | 0 | 16 | 0 | 759 | 4 | 3400 | 19 | 7392 | 68
25 | 0.46 – 0.215 eV | 0 | 0 | 0 | 0 | 14 | 0 | 620 | 2 | 3156 | 26 | 6938 | 80
26 | 0.215– 0.001 eV | 0 | 0 | 0 | 0 | 28 | 1 | 2674 | 47 | 22939 | 662 | 76253 | 3157
Average Neutron Energy |  | 13.51 MeV | 13.97 MeV | 11.47 MeV | 13.53 MeV | 9.03 MeV | 13.14 MeV | 6.83 MeV | 12.86 MeV | 4.99 MeV | 12.60 MeV | 3.53 MeV | 12.25 MeV
Diffusion/Absorption time of spectra, nanoseconds |  | 0.21 | 0.098 | 1.67 | 0.52 | 14.13 | 1.58 | 444.99 | 44.00 | 4500 | 741.72 | 19818 | 4281
Number of neutrons |  | 990995 | 9005 | 955821 | 44179 | 917945 | 82055 | 887607 | 112393 | 864222 | 135778 | 846595 | 153405

## Slide 52: Spectrums in graphite (p=2.26 g/cm3) C12 spheres
ABBN-78 Group № | Energy Interval | R = 30 cm |  | R = 40 cm |  | R = 50 cm |  | R = 65 cm |  | R = 80 cm |  | R = 100 cm | 
 |  | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum | Outgoing Spectrum | Capture Spectrum
-1 | 14.5-14.0 MeV | 16278 | 65504 | 4167 | 66796 | 1020 | 67220 | 129 | 67269 | 17 | 66876 | 0 | 67073
0 | 14.0-10.5 MeV | 59089 | 63680 | 21384 | 69082 | 7209 | 70661 | 1296 | 71634 | 183 | 71870 | 15 | 71857
1 | 10.5-6.5 MeV | 48647 | 30720 | 23925 | 35723 | 10346 | 37775 | 2669 | 38939 | 643 | 39304 | 79 | 39486
2 | 6.5-4.0 MeV | 64849 | 0 | 33686 | 0 | 15545 | 0 | 4065 | 0 | 1030 | 0 | 122 | 0
3 | 4.0-2.5 MeV | 34028 | 0 | 18747 | 0 | 8942 | 0 | 2555 | 0 | 621 | 0 | 72 | 0
4 | 2.5-1.4 MeV | 63188 | 0 | 37010 | 0 | 18803 | 0 | 5503 | 0 | 1364 | 0 | 195 | 0
5 | 1.4-0.8 MeV | 46285 | 0 | 28040 | 0 | 14393 | 0 | 4501 | 0 | 1150 | 0 | 153 | 0
6 | 0.8-0.4 MeV | 38548 | 0 | 23844 | 0 | 12629 | 0 | 3977 | 0 | 1038 | 0 | 124 | 0
7 | 0.4-0.2 MeV | 27491 | 0 | 17488 | 0 | 9547 | 0 | 3078 | 0 | 807 | 0 | 115 | 0
8 | 0.2-0.1 MeV | 21655 | 0 | 14324 | 0 | 7922 | 0 | 2582 | 0 | 725 | 0 | 95 | 0
9 | 100-46.5 KeV | 21048 | 0 | 14215 | 0 | 7744 | 0 | 2649 | 0 | 749 | 0 | 115 | 0
10 | 46.5 –21.5 KeV | 19422 | 0 | 13335 | 0 | 7395 | 0 | 2552 | 0 | 691 | 0 | 111 | 0
11 | 21.5– 10 KeV | 17730 | 0 | 12868 | 0 | 7331 | 0 | 2531 | 0 | 768 | 0 | 98 | 0
12 | 10– 4.65 KeV | 17125 | 0 | 12854 | 0 | 7256 | 0 | 2741 | 0 | 749 | 0 | 110 | 0
13 | 4.65– 2.15 KeV | 16894 | 0 | 13021 | 0 | 7702 | 0 | 2727 | 0 | 834 | 0 | 124 | 0
14 | 2.15 – 1 KeV | 16186 | 2 | 12946 | 4 | 7799 | 9 | 2796 | 5 | 820 | 10 | 133 | 10
15 | 1– 0.465 KeV | 15899 | 2 | 12866 | 11 | 7909 | 12 | 3014 | 20 | 879 | 16 | 150 | 13
16 | 465– 215 eV | 15526 | 12 | 12901 | 22 | 8048 | 20 | 3074 | 21 | 910 | 26 | 144 | 25
17 | 215– 100 eV | 14750 | 12 | 12687 | 23 | 8270 | 12 | 3091 | 31 | 1019 | 38 | 150 | 41
18 | 100– 46.5 eV | 14030 | 24 | 12841 | 31 | 8476 | 30 | 3156 | 46 | 1024 | 57 | 175 | 51
19 | 46.5– 21.5 eV | 13364 | 23 | 12727 | 49 | 8819 | 68 | 3462 | 79 | 1074 | 78 | 191 | 77
20 | 21.5– 10 eV | 12929 | 28 | 12593 | 65 | 8639 | 97 | 3509 | 121 | 1106 | 130 | 183 | 133
21 | 10– 4.65 eV | 12307 | 46 | 12524 | 96 | 8781 | 142 | 3592 | 157 | 1147 | 187 | 221 | 188
22 | 4.6 – 2.15 eV | 11799 | 78 | 12460 | 138 | 9137 | 181 | 3769 | 259 | 1312 | 275 | 220 | 265
23 | 2.1 – 1.0 eV | 11238 | 88 | 12069 | 191 | 9040 | 251 | 3855 | 308 | 1233 | 367 | 217 | 359
24 | 1.0– 0.465 eV | 10445 | 117 | 11893 | 263 | 9218 | 399 | 3979 | 454 | 1289 | 565 | 266 | 560
25 | 0.46 – 0.215 eV | 10026 | 141 | 11894 | 372 | 9291 | 593 | 4233 | 727 | 1434 | 805 | 257 | 820
26 | 0.215– 0.001 eV | 159154 | 9593 | 350289 | 37536 | 491072 | 84247 | 557249 | 177596 | 513917 | 280863 | 409606 | 590394
Average Neutron Energy |  | 2.43 MeV | 11.69 MeV | 1.10 MeV | 10.05 MeV | 484 KeV | 8.24 MeV | 135 KeV | 6.09 MeV | 36.52 KeV | 4.72 MeV | 5.66 KeV | 3.70 MeV
Diffusion/Absorption time of spectra, nanoseconds |  | 54444 | 15202 | 199367 | 77014 | 444274 | 202405 | 957056 | 476478 | 1585213 | 809223 | 2519006 | 1265172
Number of neutrons |  | 829930 | 170070 | 789598 | 210402 | 738283 | 261717 | 642334 | 357666 | 538533 | 461467 | 409606 | 590394

## Slide 53: Precision of the calculated data
Authors are interested to define precision of our calculated data, both present work describing neutron fluxes in spheres of Ta181, Ninat, C12 and already published data [8] for B10, Tinat , U238, also as [7] which describes propagation of neutron fluxes in natural isotope composition metal spheres of tungsten 74Wnat , steel 26Fenat , and sodium isotope Na23. For this purpose, we emphasized attention to value of neutron multiplication coefficient in infinitely large area of U238 for one neutron generation with fission spectrum. This important value was measured in plenty experiments with high precision and is [3, p.116] equal to 1.174.

## Slide 54: Check inside 1 meter sphere of nominal density U238 for fission neutron spectrum multiplication, showed, that initial neutron flux multiplied into 1.261915 times. Statistical precision for 1,000,000 neutrons of initial fission spectrum is better than share of delayed neutrons. Calculated leakage for central neutron source in R=1 meter U238 metal sphere is equal to 0.0031%. It’s necessary to mention, that we observe sum of all neutron generations i.e. sum of infinite geometry progression, case with K<1: Sum = 1.261915 = 1/(1-K) thus, K= 0.208 and for capture of single neutron generation we have multiplication 1.208 times. Instead of experimental value 1.174 with difference 0.034 absolute units. At the same time, authors of ABBN-78 declare precision of group constants [3, p.109] equal to (+0.04…-0.02) absolute units. Thus, precision of our calculated data was found inside interval of precision, which has implemented neutron group constants value, which is declared by it’s authors.
ABBN-78 Group № | Energy interval of energy group, MeV | Neutrons of initial fission spectrum in energy group | Sum of neutrons in all captured spectrum, produced by initial neutrons of this energy group
-1 | 14.0-14.5 | 0 | ---
0 | 10.5-14.0 | 0 | ---
1 | 6.5-10.5 | 16,000 | 36,305
2 | 4.0-6.5 | 87,000 | 141,857
3 | 2,5-4.0 | 183,000 | 272,458
4 | 1.4-2.5 | 269,000 | 358,062
5 | 0.8-1.4 | 203,000 | 210,917
6 | 0.4-0.8 | 142,000 | 142,284
7 | 0.2-0.4 | 61,000 | 61,005
8 | 0.1-0.2 | 25,000 | 25,000
9 | 0.0465-0.1 | 9,000 | 9,000
10 | 0.0215-0.0465 | 3,000 | 3,000
11 | 0.01-0.0215 | 1,000 | 1,000
12 | 0.00465-0.01 | 1,000 | 1,000
Sum of all groups | 14 Mev- 10 keV | 1,000,000 | 1,261,915

## Slide 55: Modeling results of numerical calculation shows:
1) Leakage neutron spectrum which can be measured by TOF method, and absorption spectrum, are two different neutron spectrums. In common case, they have maximum number of neutrons in different energy groups. Their correlation can be found making variant numerical calculations, especially considering, that spectrums /and their average energies, diffusion times/ changes monotonously – at least, if we speak about plenty practically important cases - during increasing thickness of substance, which the neutron flux is diffusing through.
2)
In the case of big assemblies, which radius many times exceeds transport free path of neutrons, their spectrum has average energy around 100 keV. This energy is many times smaller, than average energy of initial fission spectrum which is ~2 MeV. Such energies around ~100 KeV can be measured by existing TOF spectrometers, which have resolution factor ~ 6 nanoseconds/meter and better. This conclusion is one of practically important modeling results.
3) Substances with small absorption cross section and intermediate masses of nuclei, such as nickel 28Ni, titanium 22Ti, steel 26Fe, sodium Na23, in the case of big enough thicknesses, produce spectrum similar to spectrum Fermi. Fermi spectrum, in which neutron flux Ф~(1/E) is analytical idealization for the case, when exist no leakage and no absorption. Integration (1/E)*dE results, that if lethargy interval on energy axis is constant, then each of 28 energy groups has equal quantity of neutrons.
4) During propagating of neutrons from the center to external surface of the sphere, their average energy decrease: at first rapidly due to inelastic cross section until energy is above it’s threshold for selected nuclide. After energy becomes smaller than inelastic threshold, spectrum continues to moderate slowly due to elastic cross section. Substances like Ta181, U238, 74W which has high capture cross section in resonance neutron energy area, absorb majority of neutrons above 14th group i.e. above 1 KeV.

## Slide 56: Conclusion
1.
Integral experiments are integral check of all main types of nuclear constants, of cross sections for interaction of neutrons with nuclei, as suggested in [6]. Present work prepares calculated spectrums to compare with future experimental TOF spectra.
Such experiments can be made also with subcritical assemblies. Neutron spectrums of large fast breeder reactors with diluted fissile material has average energy around ~140 KeV. This value turns out measureable already by existing TOF spectrometers, which have resolution factor 6 nanoseconds per meter and better.
2.
Outgoing spectrum and capture spectrum differ one from another. Outgoing spectrum can be measured by TOF method, while capture spectrum is needed to calculate fast neutron reactor’s breeding ratio. Using experimentally observable TOF outgoing neutron leakage spectrum, it’s possible to reconstruct capture spectrum using numerical modeling.
3.
Due to big durations of diffusion time in the case of big assemblies, comparable to microsecond, spectrums of large subcritical assemblies with radius comparable to 1 meter, can be measured by TOF method only using long TOF bases. Their length must be several hundreds meters to provide energy resolution, high enough for spectrum average neutron energy around 140 KeV.
4.
Future work includes comparing present 28-group spectrums with 299-group ABBN-93 calculation results for their calibration. Also comparing with calculation results of codes, which use introduction of cross sections as continuous curves instead of energy groups.
5.
With statistics around 1,000,000 neutrons, providing discreteness calculation precision component better than value of delayed neutron’s share, performance of the program allows to calculate big quantity of variants using modern personal computer.
6.
Measurement of subcritical assemblies neutron spectra in 28 energy groups of ABBN-78, with TOF resolution factor 6 ns/meter, is possible. Possibility to accumulate enough statistic per energy group is also proved. At the same time, for leaking neutron flux spectra measurements in 299 energy groups of ABBN-93 system, better energy resolution factor is required.

## Slide 57: Literature
1. A.V.Dementyev, N.M.Sobolevsky SHIELD – Universal Monte Carlo hadron transport code: scope and application. Radiation Measurement 30 (1999) p.554-557.
2. https://www.inr.ru/shield
3. Л.П.Абагян, Н.О.Базянц, М.Н.Николаев, А.М.Цибуля Групповые константы для расчёта реакторов и защиты. Справочник. Москва, Энергоатомиздат, 1981.
4. Manturov G.N., Nikolayev M.N., Tsibulya A.M. System of group constants ABBN-93. Part 1. Nuclear constants for calculation of neutron and photon fields of emission. VANT, ‘Nuclear Constants’, №1, 1996, p.59-98.
5. https://www.bnl.gov
6. Stavissky Yu.Ya. Neutron Research based on Moscow Meson Factory. In: ‘Program of experimental research at Meson Factory INR RAS’, volume 4, Moscow, 1986, p.7-21.
7. Sobolevsky N.M., Latysheva L.N., Djilkibayev R.M., Khliustin D.V. Evolution of the Neutron Spectrum During Propagation of the Neutron Flux in Solid Bodies. International Conference Nucleus-2024, Dubna, Russia, 2024. 8. Соболевский Н.М., Латышева Л.Н., Джилкибаев Р.М., Хлюстин Д.В. Эволюция Нейтронного Спектра при Распространении Потока Нейтронов в Боре-10, Ti и U238. IV Всероссийская научно-практическая конференция с международным участием «Задачи и методы нейтронных исследований конденсированных сред», Дубна, 2024.

## Slide 58: Session-Conference ‘Physics of Fundamental Interactions” Department of Physics, Russian Academy of Sciences. Presidium RAS, 17-21 February 2025, Moscow, Russia
Thank you for your attention!